## Slide 1
September 10th, 2013
Study of phase transformation within bimetallic rolls
Ingrid NEIRA TORRES - J. Tchoufang Tchuindjang - J. Lecomte-Beckers - G. Gilles - AM Habraken
First International Workshop. Lagashop, September 2013

## Slide 2: Introduction
Bimetallic rolling mills
High wear resistance in the shell
High toughness in the core
Studer L., 2008
Marichal Ketin industry

## Slide 3: Work motivation
High rate of failure during cooling and heat treatment for radius upper 1200mm.
Simulations using FE code will be performed in order to find the origin of the crack.
Studer L., 2008
Studer L., 2008
Fe-Pe
Ma
Studer L., 2008

## Slide 4: Model description
Contribution à la modélisation du formage des métaux par la méthode des éléments finis (A.M.Habraken, 1989)
Coupled thermo mechanical metallurgical analysis during the cooling process of steeel pieces (A.M.Habraken, M. Bourdouxhe, 1992)
Metallic structure
Temperature
Stress and strain
1 Phase transformation
2 Latent heat
3
Thermal
stress
Variation
of
mechanical
parameters
5
Heat generation
due to deformation
4
Transformation
stress and
plasticity
6
Mechanical induced
transformation
kinetic modification

## Slide 5: Model description
Thermo metallurgical model
  Heat equations
  Metallurgical model
    Transformations by diffusion (ferrite, cementite, pearlite, bainite)
      Sheil’s sum, additivity rule, TTT diagram
    Martensitic transformation
      Koistinen Marburger’s law
Modification of the thermo metallurgical model due to mechanical interaction.
Mechanical model with thermal and metallurgical interactions.
Coupled thermo metallurgic mechanical finite element

## Slide 6: Metallurgical model
Transformations by diffusion (ferrite, pearlite, bainite)
  Sheil’s sum
  TTT diagram
  Additivity rule
Martensitic transformation
  Koistinen Marburger’s law

## Slide 7: Model requirements
Lagamine
Stresses
(σx , σy ,σz , σxy)
Strains
(εth, εp, εph, εptr)
Phase rates
(%Fe, %Pe, %Ma)
Thermo physical parameters
(α, ρ, λ, Cp)
Metallurgical parameters
(TTT diagrams)
Mechanical parameters
(E, ν, Et, σy)
Analysis of results
INPUT DATA
FE code
OUTPUT DATA

## Slide 8: Sensitivity analysis
Different simulations performed in order to analyse the impact in the results.
Results published at journal “Computer methods in materials science” and presented at Komplastech conference, Zakopane, January 2013.
 | Simulation | Convection h(T) | TTT diagram | σ - ε curve
1 | Reference case | Experimental data from industry | Core: Obtained by inverse method Shell: Obtained by inverse method (Only Martensite) | Approach from available data for similar materials and experimental points
2 | Thermal modification | Constant value | Core: Obtained by inverse method Shell: Obtained by inverse method (Only Martensite) | Approach from available data for similar materials and experimental points
3 | Metallurgical modification | Experimental data from industry | Core: Slower ferritic transformation Shell: Bainitic transformation allowed | Approach from available data for similar materials and experimental points
4 | Mechanical modification | Experimental data from industry | Core: Obtained by inverse method Shell: Obtained by inverse method (Only Martensite) | Data from similar materials
Metallurgical parameters
Mechanical parameters
Thermal data
Experimental from industry. (Assaker)

## Slide 9: Summary of Results
Residual stress results
Core
Shell
Core
= Pe: 18.3% σax =
Shell
Ma: 51% σax
Core
Pe: 33% σax
Fe: 67%
Shell
Ma: 42% σax
Core σax
Shell σax =
Reference
Core = 82% Fe
18% Pe
Shell = 50%Ma
50%Au

## Slide 10: Conclusions From sensitivity analysis
Metallurgical modifications have generated the most important differences in axial stresses obtained at the end of cooling.
  Metallurgical parameters are very important to be certain
Thermal modifications through a quicker cooling have generated some effects due do the impact in phase transformations.
  Thermal parameters have been determinated through experimental tests
Mechanical parameters doesn’t have an important effect in axial stresses. However it is important in regard to the rupture criteria.
  Mechanical parameters are being experimentally determinated

## Slide 11: Metallurgical parameters
Phase transformations
Dilatation by transformation εtr
σres
TTT diagrams
CRACK
Numerical simulation to reproduce experimental curve
Unknown
Experimental dilatometric test
Thermophysical characterization
Known

## Slide 12: Dilatometry test for core material
εtr
TTT diagram
Latent heat
Thermophysical parameters
(α, ρ, λ, Cp)
Experimental data
Inverse method from CCT diagram
?
Au
Pe-Fe

## Slide 13: Dilatometry test reproduction

## Slide 14: Dilatometry test reproduction

## Slide 15: Conclusions and perspectives
Thermo mechanical metallurgical simulations are possible to be performed using Lagamine code, allowing to estimate stresses and strains generated in the rolls during cooling or heat treatment.
Metallurgical parameters are highly important
Lagamine code has been also useful to estimate the unknown value of the parameter εtr.
It is also possible to use Lagamine code in order to reproduce another experimental tests such as compression tests in order to optimize the experimental conditions.

## Slide 16: Thank you for your attention