## Slide 1: A multi-step process for an alternative wheat bran biorefinery
Hemicellulose: 47%
Cellulose: 15%
Lignin (van Soest): 8%
Proteins: 12%
Wheat bran (WB) is a highly available and cheap agriculture byproduct that constitutes a feedstock of choice for biorefineries. Classical WB biorefining is premised on the fermentation of the monosaccharides from starch and hemicellulose into fuel and chemicals. Here is presented an alternative concept based on a multi-step process aiming at the production of three fractions with high added-value from destarched wheat bran (DWB).
After WB destarching (10 min in water at 95 °C), the DWB underwent an extraction of its arabinoxylans (AXs), then in a second step its lignin was recovered, leaving a solid residue rich in cellulose which could be further bleached and hydrolysed.
© CBI – Gembloux Agro-Bio Tech – Université de Liège
Mario Aguedoa*, Christian Fougniesb, Aurore Richela aUnit of Biological and Industrial Chemistry, Gembloux Agro-Bio Tech - University of Liège, 5030 Gembloux, Belgium
bCosucra Groupe Warcoing S.A., Rue de la Sucrerie 1, 7740 Warcoing, Belgium *mario.aguedo@ulg.ac.be
Unit of Biological and Industrial Chemistry Passage des déportés, 2 5030 Gembloux Tel: +32 81 62 22 31
© 2014 CBI - Gembloux Agro-Bio Tech - Université de Liège
www.gembloux.ulg.ac.be/chimie-biologique-industrielle
Unit of Biological and Industrial Chemistry
Unit of Biological and Industrial Chemistry
DESTARCHED WHEAT BRAN
LIGNIN
CELLULOSE
HEMICELLULOSE
Step 1 : Extraction of arabinoxylans (AXs)
This study was financially supported by the Walloon Region through BARCELONE project (number SPW 6511)
Step 3 : Obtaining of a cellulose fraction
Step 2 : Extraction of lignin
DWB
0.44 M NaOH, 80 °C/15 h, under srring
AXs
AXs + AXOS (AX-oligosaccharides)
Deesterified Axs, Molecular mass >670 kDa Arabinose/xylose ≈ 1
+ ≈ 7% proteins
Esterified Axs,
2 populations: one main with mol. mass ≈ 5-12.5 Da and a smaller one at 140-160 kDa
Arabinose/xylose ≈ 0.5
+ ≈ 7% proteins
EDWB
(=DWB exhausted in extractable-AXs)
Solid residue
Solid residue
Food grade
commercial
prebiotic AXOS
Green polymers for: materials, cosmetics, pharmaceutics,
food,…
High-purity lignin for potential high-added-value applications in materials…
Properties to be tested
Cellulose: 50%
Lignin (Klason or van Soest): 30-31%
Hemicellulose: <2%
Water, pH 5, Thermal reactor, 5 °C/min to 180 °C/3 min, 3 times
Ethanol precipitation, filtration 25 μm
Solid residue
Hydrothermal treatment in reactor: heating at 148 °C/5 min,
in ethanol/water/H2SO4 6 M (18.4/0.53/1.07)
Cellulose-rich residue
Cellulose: 80-90%
Lignin (van Soest): <0.5%
Hemicellulose: <2%
Proteins: 5-6%
NaOH 30%, 80 °C/30 min
Bleaching (H2O2 3%/NaOH pH 11.5, 1 h)
Cellulose
85-95%
Cellulose
85-95%
Hydrolysis HCl 9%, 30 min/100 °C
Cellulose with increaded crystallinity
Conclusions
FD100* (80-90% cryst.)
C200* (50-60% crystallinity)
Bleached and hydrolysed with HCl
NaOH-treated and hydrolysed with HCl
Typical shoulder from crystalline cellulose
Crystallinity by RX-Diffraction:
*commercial cellulose
Here is described an up-scalable multi-step process that could constitute an alternative biorefinery approach to recover high added-value products from wheat bran. Thus, AX fractions of various molecular masses, a high-purity lignin and cellulose fractions of various qualities can be obtained with good yields from destarched wheat bran. The biomass treatments used NaOH and fast and efficient thermal heating; the whole process yields marketable bio-based polymers.
SEM image
Lignin
X
Organosolv (107 ºC / 3 or 4.5 h)
formic acid/acetic acid/water (20, 30,40/40, 50, 60/20)
No efficient lignin extraction
Mol. mass ≈ 1-2 kDa (THF as eluent by laser light scattering)
Saccharides (gluc.) ≈ 1-3%
Proteins ≈ 2.4-8%
Syringyl/Guaiacyl/p-Hydroxyphenyl ≈ 3.9/3.6/1
Marketable cellulose fractions for: cosmetics, pharmaceutics, materials, food,…
100
~20
~15-20
~30
~8
~20-25
~15-25
~13-15
Yields
~5-10