## Slide 1: From Geometallurgy to Ecometallurgy Building mines for the future
Eric PIRARD Dr. Ir.
Rafaël CONTRERAS, Godefroid DISLAIRE, Laura PEREZ-BARNUEVO,
Xavier DECAMP, Maxime EVRARD, Sophie LEROY, Pierre BARNABÉ, Fanny LAMBERT, David BASTIN

## Slide 2: GeMMe
Minerals Engineering, Materials & Environment
GeMMe operates on the characterization, beneficiation, transformation, use and recycling of mineral materials at any stage of their life cycle.
INNOVATION
CReSus
Centre for Resource Efficiency & Sustainability
RESEARCH
EDUCATION

## Slide 3: Applied Mineralogy Choosing the right perspective

## Slide 4: Applied Mineralogy
What is a mineral ?
  Dana’s definition encompasses :
    Naturally occurring
    Stable at room temperature
    Represented by a chemical formula
    Usually abiogenic
    Ordered atomic arrangement
  Nickel,E. (IMA 1995)
    A mineral is an element or chemical compound that is normally crystalline and that has been formed as a result of geological processes.
  … and industrial processes
    Addition needed for process and applied mineralogists
    ex. Wüstite FeO
      named for Fritz Wüst (1860–1938), a German… metallurgist (not Ewald the geologist)
Choosing the right perspective

## Slide 5: Applied Mineralogy
A DIAGNOSTIC perspective
  Geology
    Chemical and mineralogical analysis for each rock specimen
    Occurrence of a particular and very rare mineral => (P,T°)
    Can only observe the final result (output).
    Speculation about the geological process
A geologist can (sometimes) extract pertinent information from the smallest and most exotic features!
Wüstite from Sikhote-Alin © Kartashov
Choosing the right perspective

## Slide 6: Applied Mineralogy
A DIAGNOSTIC perspective
  Process Mineralogy
    Unit process monitoring
    Input/Output analysis
      Differences intepreted in terms of process impact / deficiency,…
Choosing the right perspective
A process mineralogist is interested by microscopical properties of materials daily fed to the plant in thousands of tons!
© JF Douce, ArcelorMittal
Microspecular(granular) : < 20 µm grains
Recrystallized : < 50 µm irregular grains
Sinter with relict Hem, Mgt + Neoformed Hem + Ca ferrites + Si glass
Critical sampling issues!
Do more less well

## Slide 7: Applied Mineralogy
A PROGNOSTIC perspective
  Geometallurgy
    Deposit
      Regional Variability,…
      Zonation, stratification,…
      Faults, Geomechanical testing,…
    Rock/Ore
      Local Variability,…
      Grade and Mineralogy
      Pores, Fractures, Grain size, shape, arrangements, …
      Mineralurgical testing,…
    Particulate system
      Interparticle variability (Liberation)
      Microchemical probing,…
Choosing the right perspective
A geometallurgist gathers quantitative data as input to models for predicting behaviour in several industrial processes (blasting; grinding; leaching; flotation;…)
He considers valuable, deleterious and gangue-forming minerals
Sampling, Geostatistics and Stereology:
  3D from cores
  3D from sections
  3D from tomography

## Slide 8: Geometallurgy Developing the right tools

## Slide 9: Geometallurgy
Macro scale (Deposit)
  Opto-Mechanical Core-scanning
    Decamp X., Barnabé P., Pirard E., IMA (2014) LITHOLOGICAL MAPPING FROM OPTICAL & MECHANICAL MEASUREMENTS HYPERSPECTRAL IMAGING & 3D SENSING
Developping the right tools
EPSLOG
Co-registered diffuse reflectance imaging
Cam 1 : 400 nm - 1000 nm
Cam 2 : 970 nm – 2500 nm
Scratch test

## Slide 10: Geometallurgy
Macro scale (Deposit)
  3D chips scanning
    Destructive drilling generate cuttings whose size and shape can be used to estimate tensile and shear type failure modes.
    3D image analysis of chips induced by core scratch testing indicate strong correlations with the intrinsic grain size and the cutting depth
    Pirard, E. et al., WCPT Nürnberg (2010) 3D AND 2D PARTICLE IMAGE ANALYSIS OF ROCK CHIPS GENERATED BY CORE SCRATCH TESTS
Developping the right tools
EPSLOG

## Slide 11: Geometallurgy
Meso scale (Rock/Ore)
  Multiradial Microscopy
    Contreras R., Pirard E., S4G Prague (2012) FABRIC ANALYSIS OF CARBONATE ROCKS USING MULTIRADIAL IMAGING AND INTERCEPTS
Developping the right tools
Multiradial Image
Porosity
Grain Boundaries (gradient)

## Slide 12: Geometallurgy
Meso scale (rock)
  Multiradial Microscopy
    Crystal Size Distribution to predict decrepitation
Developping the right tools
Percentiles of Intercept Length (Crystal Size CSD)

## Slide 13: Geometallurgy
Micro scale (particle)
  MicroTexture Indices
    Perez-Barnuevo L., Pirard E., Castroviejo R. Min. Eng. (2013) AUTOMATED CHARACTERISATION OF INTERGROWTH TEXTURES IN MINERAL PARTICLES
Developping the right tools

## Slide 14: Geometallurgy
Micro scale (particle)
  MicroTexture Indices
    Perez-Barnuevo L., Pirard E., Castroviejo R. Min. Eng. (2013) AUTOMATED CHARACTERISATION OF INTERGROWTH TEXTURES IN MINERAL PARTICLES
Developping the right tools
CC-STWK
CC-MIX
CC- RIM
LIB CP
CC-MIX
CC-STWK
CC-RIM
Ex_Class
CC-RIM+STWK
Kansanshi Mixed Zone

## Slide 15
WEEE sculpture (Eden Project, UK)
From Geometallurgy to Ecometallurgy Getting ready for a new cycle

## Slide 16: Ecometallurgy
From Georesources to Ecoresources
Getting ready for a new cycle

## Slide 17: Ecometallurgy
Material Centric Perspective
  Aluminium life-cycle
Getting ready for a new cycle
Cradle-to-cradle © ALCOA
Al
Al
Ga

## Slide 18: Ecometallurgy
Product Centric Perspective
  Cellphone life-cycle
Getting ready for a new cycle
End of Life
Disassembly
Shredding
Screening
Sorting
Pyrometallurgy
Hydrometallurgy
Outotec TSL
© Reuter 2011
Cu, PM
Slag
Flue dust
Complex Leachate
Cu
Pb
PM
Zn
RE
Ga
Ta
Li
…

## Slide 19: Evolution of Products
Future products will not only be optimized with regard to their functionality but also their recyclability and the sustainable availability of resources
Is this progress ?
Incandescent
12-20 lm/W
Halogene
18-25 lm/W
Fluo-compact
60-80 lm/W
LED
25-140 lm/W
Tungsten
Iodine, Bromine, …
Glass,…
Tungsten
Mercury, Rare Earths,… Glass, Plastics,…
Gallium
Indium, Cerium, Yttrium, Copper, Silver, Silicium, …
Plastics, …
Tungsten
Glass,…

## Slide 20: Building Mines for the Future
Metal concentrations
  Maintain grade above a technological cut-off
Metal speciation
  Metal, alloy, salt , organic compound,…
Metal paragenesis
  Unexpected metal assemblages,…, contamination
Textural assemblage
  Liberation and dismantling
Volume of mine
  Make sure large enough quantitities can be collected
Homogeneity
  Zonation, Blending
Ecometallurgy

## Slide 21: Building Mines for the Future
Metal concentrations in Urban Mines
  Maintain grade above a technological cut-off
    Often only precious metals (Au, PGM) pay for recycling
  Composition of PCB
    Base metals (35%): Cu, Zn, Al, Pb, Sn, …
      Rare Metals
        Au 100-1000g/t
        Ga 30g/t; In 30g/t; Nd 300g/t
    Cellphones : 50 g/t Ga
      Up to 1000 g/t Ga in IC
      How to separate IC from PCB ?
    Ge doped optical fibers (14mg/km)
    Ge lost in PET bottles (dispersive use)
Ecometallurgy

## Slide 22: Building Mines for the Future
Metal speciation
  Metal, alloy, salt , organic compound,…
    Wide variety of alloys (Ni, Al,…)
    Hard to separate by physical means (=> innovative optical sorting needed)
Metal paragenesis
  Unexpected metal assemblages
    Copper coated aluminium wires
  Association with deleterious elements
    InGaAs
    As toxic, low value, impacts process costs
Textural assemblage
  Liberation and dismantling
    Separate core from cladding and jacket in optical fibers
    Need for « design for recycling »; smart joints;…
Ecometallurgy

## Slide 23: Building Mines for the Future
Volume of mine (resource evaluation)
  Make sure large enough quantitities can be collected
    Collectables not collectibles
    Infrastructure (lighting LEDs), Building (Electric wires; Cu tubes),… (OK)
    Specialized IR lenses; (?)
  Urban mines are mobile
    Tax, legislations, trading,…
Homogeneity of the deposit (4D+ problem)
  Zonation, Blending
    Technological evolution with time changes deposit
      From Compact Fluo lamps to LEDs !
    Need for flexible and adaptive processing plants
Ecometallurgy

## Slide 24: Perspectives
Resource Efficiency
  Mineralogists and geologists have to contribute to a « resource efficient » society
  Excellent background to adress the circular economy (LCA, MFA,…)
    Resource characterization & Evaluation
    Predictive approach to processing
Education
  Multidisciplinary training
  From « geology to mineral processing »
  From « orebody modelling to metallurgical simulations »
  EMerald Master in Georesources Engineering
    Liege > Nancy > Lulea > Freiberg
Geo/Ecometallurgy
www.em-georesources.eu

## Slide 25: Perspectives
Creating KICs « Knowledge Innovation Communities »
  European Raw Materials Initiative
  EIT call for a KIC on Raw materials: sustainable exploration, extraction, processing, recycling and substitution
  250 M€ + for innovation
Geo/Ecometallurgy
EU Decision 09 DEC 14

## Slide 26: Thank You
See you in Liège, 2015
Liège, Belgium
Session 11 : Geometallurgy (Pirard, Lamberg, Bradshaw)
Exploring new dimensions in imaging…