## Slide 1: Mineralogy of fine particles in slurry from multispectral imaging
Sophie LEROY
G. Dislaire, P. Barnabé, E. Pirard

## Slide 2: University of Liège (BE)
Predictive Mineralogy
Process Control
Exploration
Remote Sensing
Reserve Estimation
Georesources & Geo-Imaging Research Group
© CSIRO
Quantitative Microscopy
On Line Vision
Core Scanning
3D particle size & shape

## Slide 3: 2D Particle Imaging
Range 50µm -> 5mm+
    104 particles/min
  Mechanical dispersion
    Vibration (tray)
    Acceleration (conveyor)
  Suction
    Laminar air flow
Free flowing powders

## Slide 4: 2D Particle Imaging
Range 500nm - 150µm+
    105 particles / min
  Vacuum dispersion
    For dry powders
  Flow cell
    For wet powders suspensions emulsions,…
Non free flowing powders

## Slide 5: 2D Particle Imaging
Estimation of chromite content in UG2 slurries
  Modified flow cell
    Identification of chromite grains (opaque)
    Real time estimation of chromite content and liberation
Size and Mineralogy
[chromite] from AA
[chromite] from IMAGE

## Slide 6: Reflectance of particles
Existing spectral databases
  Specular reflectance of ore-forming minerals
    QDFIII 400nm-700nm (Criddle & Stanley, 1993)
    Extended to 1000nm (Brea et al., 2010)
Mineralogy & Particle Size

## Slide 7: Reflectance of particles
Existing spectral databases
  Diffuse reflectance of rock forming minerals
    Speclab USGS, Grove et al. (1992)
Mineralogy & Particle Size
< 45 µm
< 125 µm
< 500 µm
Chalcopyrite
Pyrite
Specular (QDFIII)

## Slide 8: Imaging System
Best of both worlds
  Diascopic imaging for opaques
    White LED illumination
  Episcopic imaging
    Selected LEDs
      Eight wavelength
    Dichroic mirrors
    Dark field objective
Multispectral Set Up

## Slide 9: Imaging System
Gangue Silicates vs Sulphides
Diascopic Imaging

## Slide 10: Imaging System
Oxides vs Sulphides
Episcopic Darkfield RGB Imaging

## Slide 11: Imaging System
Chromite vs Pyrite
  Photonfocus MV1 D1312ie
    1312x1082 (binning)
    3,1 µm/pixel
    400 ms
Episcopic Darkfield Spectral Imaging
Backlit image
F0=405 nm
F1=455 nm
F3=590 nm
F4=617 nm
F2=530 nm
F5=735 nm
F6=950 nm

## Slide 12: Mineralogical Mapping
Darkfield imaging
  Reflectance angles
    Maximum reflectance depends on particle shape and λ
Calibration and discrimination
Cu wire Ø=100 µm

## Slide 13: Mineralogical Mapping
Darkfield imaging
  Pyrite vs. Copper
    Percentile P80 of intensity distribution within particle
      Combination of > P80 per wavelength
Discrimination
Pixels voted > P80 for every λ
Pyrite Ø=52 µm
Mask
P80
Cu wire Ø=100 µm
P80
P99
Raw spectrum
Raw spectrum

## Slide 14: Test on Sulphide Slurries
LYSC: Pyrite-rich (> 91%)
LYSB: Mixed sulphides (Py+Cp+…)
Particle sizing vs. 405nm/617nm band ratio
Discrimination
Pyrite-rich (LYSC )
Mixed sulphides (LYSB)

## Slide 15: Test on Sulphide Slurries
LYSC: Pyrite-rich (> 91%)
LYSB: Mixed sulphides (Py+Cp+…)
Particle sizing vs. 455nm/617nm band ratio
Discrimination
Pyrite-rich (LYSC )
Mixed sulphides (LYSB)
Py
Cp

## Slide 16: Test on Sulphide Slurries
LYSC: Pyrite-rich (> 91%)
LYSB: Mixed sulphides (Py+Cp+…)
Particle sizing vs. 405nm/617nm band ratio
Discrimination
Pyrite-rich (LYSC )
Mixed sulphides (LYSB)
Grey sulphide (sphalerite, galena, arsenopyrite,…) (tbc)
Yellow sulphides mix (pyrite,chalcopyrite,…)

## Slide 17: Conclusions
Improved flow cell imaging system
  Combined dia- and episcopic imaging
  Particle size, shape + mineralogy, (liberation)
Multispectral imaging
  Simple and flexible
  Tunable to dedicated minerals
Image processing
  Spectra of brightest pixels (> P80) to limit size and shape influence
Mineralogy
  Band-ratio discrimination
Online mineralogy

## Slide 18: Perspectives
Mineralogical Analysis
  Needs further calibration
  Cross-validation with chemistry and XRD
Discrimination limits
  Gangue
    Carbonates vs. Silicates
  Sulphides
    Cp, Py, Ga, Sp, Po,…
  Oxides
    Hem vs. Goe; Ilm vs. Lcx vs. Rut; …
Sample Preparation
  Dilution needed for dirty and dense pulps
Multimodal imaging
  Add other imaging modules (i.e. SWIR, Raman,…)
Online mineralogy

## Slide 19: Thank You
See you in Liège in 2015
www.em-georesources.eu
Liège, Belgium