## Slide 1
5. ORR activity
The catalytic layers used in proton exchange membrane fuel cell (PEMFC) are classically based on Pt particles supported on a high surface area carbon (HSAC). The structure of these catalytic layers is however not optimal, resulting in incomplete utilization of the mass of Pt loaded onto the carbon support [1]. To reduce the cost of the catalytic layer without decreasing its performance, two parameters can be improved: the support and the metallic particles. The properties of commonly used carbon blacks, as described by Rodríguez-Reinoso [2] are not optimal for electrocatalysis. A possible solution to these drawbacks is to use synthetic nanostructured materials with a controllable, reproducible texture and with a pure, known and constant chemical composition; carbon xerogels (CX) exhibit such properties [3]. Highly dispersed CX-supported Pt nanoparticles catalysts (Pt/CX) have been synthesized via formic acid (HCOOH) reduction inspired from a previous work of Alegre [4]. However, the decrease of the Pt mass contained in the PEMFC electrodes, in particular at the cathode where the oxygen reduction reaction (ORR) occurs, remains a major challenge. Improving the ORR mass activity is currently best achieved by alloying Pt with 3d-transition metal atoms such as cobalt (Co). These alloys show better ORR performance due to the substitution of some Pt atoms by 3d-metal atoms with smaller radius, which leads to a modified Pt electronic structure [5]. Bimetallic catalysts (PtCo3/CX) were synthesized via a new method using trisodium citrate in order to obtain core@shell or hollow particles. These particular nanostructures could induce an increase in mass activity for the ORR.
The Tanaka 37 wt.% Pt on HSAC, i.e. the commercial catalyst used as reference, and the 18 wt.% Pt/CX catalyst display similar average particle diameter, 3.1 and 2.8 nm respectively, and the same standard deviation, 1.1 and 1.0 nm. The 39 wt.% Pt/CX catalyst presents a slightly higher particle diameter, 3.6 nm, with the same standard deviation, 1.2 nm. A combination of core@shell and hollow nanoparticles was obtained for the PtCo3/CX catalysts with a diameter of ca. 47 nm. Such nanoparticles were synthesized by the formation of a Co core followed by the deposition of a PtCo shell by (i) galvanic replacement and (ii) chemical reduction of Pt and Co by NaBH4. The Pt/CX and the PtCo3/CX catalysts have a higher specific and mass activity toward the ORR than the Tanaka 37 wt.%. This can be explained by (i) an improved nanoparticle distribution on the support, CX instead of HSAC, (ii) a modification of the Pt electronic structure induced by Co atoms (for the PtCo3/CX catalyst) and (iii) the core@shell – hollow morphology. These results, obtained by a new synthesis process using trisodium citrate, are promising. Further experiments are planned by our groups to optimize the nanoparticles morphology and activity.
1. Commercial Catalyst
[1] H. A. Gasteiger, et al. Appl. Catal. B : Environmental 56 (2005) 9-35. [2] F. Rodriguez-Reinoso, in: Porosity in carbons, J. W. Patrick (Ed.), Wiley, UK, 1995, p.153. [3] N. Job, et al. Carbon 43 (2005) 2481. [4] C. Alegre, et al. Appl. Catal. B : Environmental 147 (2014) 947-957. [5] J. R. Kitchin, et al. Journal of Chemical Physics 120 (2004) 10240.
18 wt.% Pt/CX (top) and 39 wt.% Pt/CX (bottom) synthesized by HCOOH reduction TEM micrographs
10 wt.%Pt PtCo3/CX-A (top) and
10 wt.%Pt PtCo3/CX-B (bottom) TEM micrographs
Synthesis and characterisation of
Pt-Co/carbon xerogel electrocatalysts
for Proton Exchange Membrane Fuel Cells (PEMFC)
A. Zubiaur*1, T. Asset1,2,3, P.-Y. Olu1,2,3, L. Dubau2,3, F. Maillard2,3, N. Job1
1 Department of Chemical Engineering – Nanomaterials, Catalysis, Electrochemistry, University of Liège, 4000 Liège, Belgium
2 CNRS, LEPMI, F-38000 Grenoble, France
3 Univ. Grenoble Alpes, LEPMI, F-38000 Grenoble, France
(*Contact: a.zubiaur@ulg.ac.be)
50 nm
50 nm
50 nm
50 nm
Core@shell
particle
Hollow
particles
4. Particle size
Chart: jspe / A/m²Pt
| 0.9 V | 0.85 V
Tanaka 40% | 0.221 | 0.461
18% Pt/CX | 0.437 | 0.703
39% Pt/CX | 0.609 | 2.04
10% Pt3CO/CX-A | 4.05 | 12
10% Pt3CO/CX-B | 4.3 | 15.4
Chart: jmass / A/gPt
| 0.9 V | 0.85 V
Tanaka 40% | 12.597 | 26.277
18% Pt/CX | 28.842 | 46.398
39% Pt/CX | 28.623 | 95.88
10% Pt3CO/CX-A | 81 | 240
10% Pt3CO/CX-B | 81.7 | 292.6
Specific activity and mass activity for the ORR at 0.9 and 0.85 V vs. RHE in 0.1 M HClO4
6. Hollow particles
EDX line-scans and HAADF image of a single PtCo hollow particle, the profiles show Pt (red profile) and Co (green profile) over the entire particle.
Higher specific and
mass activity
Less platinum
50 nm
Tanaka 37 wt.% Pt/HSAC TEM micrograph
Catalyst | dTEM (nm) | σ (nm)
Tanaka 37 wt.% | 3.1 | 1.1
18 wt.% Pt/CX | 2.8 | 1.0
39 wt.% Pt/CX | 3.6 | 1.2
10 wt.%Pt PtCo3/CX-A | 47.8 | 2.6
10 wt.%Pt PtCo3/CX-B | 45.8 | 2.0
Tanaka 37 wt.%
18 wt.% Pt/CX
39 wt.% Pt/CX
10 wt.%Pt PtCo3/CX-A
10 wt.%Pt PtCo3/CX-B
1. Commercial catalyst
2. Pt/CX catalysts
3. PtCo3/CX catalysts
4. Particle size
*
* Some agglomerates were observed