High-temperature and quantitative XRD study of typical Westerwald clays (Germany)

F. Fontaine1*, N. Fagel1

1AGEs, Argiles, Géochimie et Environnement sédimentaires, Université de Liège, Liège, Belgium

* Corresponding author: f.fontaine@ulg.ac.be

Keywords: Westerwald, XRD, QPA, HTXRD

The Westerwald region is one of the largest and oldest clay mining area of Germany. Those deposits were formed during the Eocene and Oligocene as a result of the weathering, erosion and redeposition of Devonian rocks. During the Miocene, intense volcanic activities led to a large basalt cover, protecting the clays from the erosion. The fine fraction is mainly composed of kaolinite and illite, with the possible presence of interstratified I-S. Other minerals such as quartz, feldspars, hematite, goethite or anatase are present in variable concentrations.

Four typical Westerwald clays were chosen for this study: kaolinite-rich clay, kaolinite-illite clay, a red and a yellow firing clays. The first goal is to perform quantitative XRD using two different methods and to compare them: reference intensity ratio (RIR) and Rietveld (using Topas and BGMN). The second goal is the study of those samples using high-temperature XRD (HTXRD). The samples were heated up to 1250°C and a XRD pattern was obtained in situ every 100°C. The results show the temperatures of vitrification and formation of mullite and cristobalite varying from one sample to another, which is mainly linked to their flux concentration.