## Slide 1
ASC September 2016
Xavier D.A. Baumans
Experimental Physics of Nanostructured Materials
Physics Department, University of Liège
BELGIUM
Ultra-narrow superconducting junctions: electromigration to shed light on quantum point contacts

## Slide 2
Collaborators
A. V. Silhanek, O.-A. Adami (ULg, BE)
V. S. Zharinov, D. Cerbu, N. Verellen, J. E. Scheerder, G. Zhang, V. V. Moshchalkov, J. Van de Vondel (KULeuven, BE)
G. Papari (U. Federico II and CNR-SPIN, Naples, IT)

## Slide 3
Context and Motivation
nm
[1]
Promising future for nanoscale superconductors …
High temperature superconducting state with
≳ 100 K in Al nanoclusters [2]
[1] Croitoru et al., Phys. Rev. B 76, 024511 (2007) | [2] Halder et al., Nano Lett. 15, 1410 (2015)
Notes: Halder= It has been predicted that as a result of the shell levels’ high degeneracy, nanoclusters composed of just tens to hundreds of atoms can display pair correlations associated with the superconducting state. For certain sizes and materials, the pairing may become exceptionally strong. Al cluster with 66 atoms.

## Slide 4
Threaten by fluctuations …
Arutyunov, Golubev, Zaikin, Physics Reports 464, 1 (2008)
Context and Motivation
TPS
QPS
Notes: If T0 then TPS play no role, but QPS are T independent and they are finite even at T=0.
Making sigma small we increase both TPS and QPS probability, but still at very low T, TPS are negligible while QPS not.

## Slide 5
Evidence of TPS to QPS transition requires going beyond EBL resolution…
Zgirski et al., Nanoletters 5, 1029 (2005)
Ar+ ion sputtering for progressive reduction of an Al nanowire effective cross section down to few nm
Tape peel-off technique
Al and MoGe
w=20 nm and L > 80 nm
Bae et al.,
Nanoletters 9, 1889 (2009)
See also Altomare et al., Appl. Phys. Lett. 86, 172501 (2005)
Giordano et al., Phys. Rev. Lett. 43, (1979)
Notes: In recent works, Bezryadin-Tinkham carbon nanotubes of width 10 nm were used as substrates supporting MoGe superconducting film.

## Slide 6
Uncontrolled electromigration
An alternative technique: electromigration
voids
formation
T
dR/dt
current
crowding
Resistance
Current
Ho & Kwok, Rep. Prog. Phys (1981)

## Slide 7
Controlled electromigration
Resistance
Current
voids
formation
T
dR/dt ~ const.
current
crowding
Z = 2 mm
W1= 150 nm
W0 = 50 nm
See Campbell, J. M. & Knobel, R. G. Appl. Phys. Lett. 102, 023105 (2013)

## Slide 8
ΔF
X. D. A. Baumans et al., Nat. Commun. 7, 10560 (2016)
Φ
Φ+2π
R(T) evidence the TPS to QPS transition
Notes: Rq=6,5 kOhms  single conduction channel, possibly single atom.

## Slide 9
R(T) evidence the TPS to QPS transition

## Slide 10
Healing via anti-electromigration
After healing
I
Anti-Electromig.
Before healing
I
Electromigration
I
I
Ittah et al. Nano Letters (2008) | Xiang et al. Nano Letters (2009)
10

## Slide 11
Conclusion
Electromigration is a promising method to create superconducting nanostructures beyond EBL resolution
R(T) evidence the transition from TPS to QPS
Negative Magnetoresistance as a side effect of different Tc of the contact leads
V(I)s measurements and the statistical distribution of critical current reinforce the evidence of TPS-QPS transition.
Upcoming
Notes: It is possibility to obtain atomic size constrictions.
The EM process has certain degree of reversibility down to few Ohms

## Slide 12
Acknowledgements

## Slide 14
X. D. A. Baumans et al., Nat. Commun. 7, 10560 (2016)
R(B): NMR and phase slips

## Slide 15
X. D. A. Baumans et al., Nat. Commun. 7, 10560 (2016)
R(B): NMR and phase slips
JT
JS ~ JT
JS << JT

## Slide 16
X. D. A. Baumans et al., Nat. Commun. 7, 10560 (2016)
R(B): NMR and phase slips
HC2

## Slide 17
X. D. A. Baumans et al., Nat. Commun. 7, 10560 (2016)
Quantum Point contact
Similar effects reported by
A. Bezryadin, C. N. Lau & M. Tinkham
Nature (2000) in MoGe nanowires
Theory for JJ
Penttilä et al. PRL (1999)
Notes: The insulating state is delocalized in the phase-space and localized in the charge space, meaning localization of the Cooper pairs.
A bias voltage weaken the charge-localization effect, leading to the observed reduction in the differential resistance

## Slide 18
Constant power electromigration

## Slide 19
kBT
Dj
0
2p
DF
Energy

## Slide 20
IC distributions

## Slide 21
200 µm
20 µm
I+
I-
V+
V-
1 µm
50 nm
(a)
(b)
(c)
(d)
Si
Al

## Slide 22
X. D. A. Baumans et al., Nat. Commun. 7, 10560 (2016)
R(B): NMR and phase slips
HC2

## Slide 23
200 µm
I+
I-
V+
V-
(a)
1 µm
50 nm
(c)
(d)
20 µm
(b)
Si
Al
(e)
(f)

## Slide 25
Results
Critical current (IC)

## Slide 26
Results
IC(T): another point of view on TAPS/QPS crossover

## Slide 28
The PID controller has a bandwidth of 100 kHz, which allows for small corrections to the device voltage at a rate much faster than what is provided by the software feedback.
The PID controller (SRS-SIM960) monitors the voltage across the
point contact junction as measured with a differential amplifier (Signal Recovery 5113 pre-amp) and adjusts its output to keep this voltage at a given
setpoint. The voltage across the junction as well as the current through it are
monitored by a computer, which then controls the PID setpoint according to the feedback algorithm.