## Slide 1
Since different detection formats are combined in the same sensor chip
δλ~16 nm
Wavelength, nm
Ellipsometric angle Ψ, °
Hybrid plasmonic multichannel spectroscopic sensor platform
Centre Spatial de Liège (ULiège) / Surface Micro & Nano Engineering
Liège Science Park, Avenue du Pré-Aily; B-4031 ANGLEUR (Belgium), Tél: +32.4.382.46.00; Fax: +32.4.367.56.13; e-mail: kfleury@ulg.ac.be ; http://www.csl.uliege.be
1. What is our instrumental concept?
2. What is the goal of our instrumental approach?
One biosensor channel = SPR / LSPR sensor + Fiber Spectroscopic channel
3. First proof-of-concept experimental investigations
ACKNOWLEDGEMENTS: This research is conducted in the framework of the “BIOSENS" project (SMARTBIOCONTROL portfolio) in the INTERREG program involving financial support from the European Union and the Walloon region.
Experiment in good agreement with theory
SEM image
Wavelength, nm
Extinction coefficient
Wavelength, nm
Normalized absorption
Experiment
Transmission and extinction spectra for two test liquids :
nD = 1.332
nD =1.3469
Two detection formats on the same lab-on-chip device: SPR & LSPR
LSPR detection spots locally synthesized using laser direct writing
LSPR detection in Total Internal Reflectance (TIR) mode
δλ~2 nm
Fine metrology involving SEM & AFM reveals:
High reproducibility of the NPs shape and density
NPs typical size ~30 nm, max range : 10-70 nm
NPs free space excitation via propagating wave:
Abstract: we present a hybrid plasmonic sensor concept, as well as the first proof-of-concept experimental investigations, demonstrating its practical feasibility. The proposed approach gives access to two detection formats on the same lab-on-chip device: surface plasmon resonance (SPR) and localized surface plasmon resonance (LSPR) biosensing . The developed instrumental platform is dedicated to multichannel biosensing. In order to implement the proposed sensing approach, we developed a specific microfabrication technique involving gold nanoparticles (Au_NPs) synthesis by pulsed laser writing followed by annealing. This technology provides powerful tools for flexible patterning of the microfluidic sensor chips with array of different SPR and LSPR probes.
The optical properties of synthesized NPs have been investigated using specially developed equipment involving total internal reflectance ellipsometric spectroscopy (TIR_ES). We experimentally demonstrate that the use of the TIR-based optical readout can significantly enhance the LSPR sensor sensibility to refraction index variations of the liquid sample.
The wavelength interrogation in TIR mode is very promising alternative to enhance the LSPR biosensing sensitivity
!
Conclusion:
Concept of the biochemical hybrid multichannel sensing platform is under development;
Bio-sensing involving LSPR_TIR detection format is proposed and experimentally investigated
First experimental results are obtained : an enhanced sensitivity of LSPR_TIR sensing in comparison to LSPR in transmission mode is experimentally demonstrated
NPs size distribution
3.2. Laser synthesized NPs properties:
Extinction cross section ≈ Absorption cross section
Refractive index sensitivity of LSPR sensor ~ 90 nm/RIU
Specular light intensity monitoring
The most appropriate format for LSPR sensor interrogation:
4. First sketch of the sensor design
Wavelength
Intensity
Index changes
SPR / LSPR sensor spots
Monitored wavelength spectra
Collimators
Microfluidic sensor chip
Multichannel Fiber Spectroscope
Optical coupler (embossed micro-prisms, … )
Polychromatic TM-polarized light wave source (s)
NPs excitation via evanescent optical field in Total Internal Reflectance (TIR):
3.3. LSPR spectra measured for different liquid samples:
Theory (Mie)
δλ~2 nm
Ellipsometric data acquired at a fixed incidence angle of 73°
    Large amount of information on the liquid sample
    High degree of miniaturization for the plasmonic multichannel sensor
    Relative simplicity of fabrication in large bi-dimensional array of LSPR sensors adapted to microfluidic system architecture
  Additional advantages: the wavelength spectrum is not perturbed by light reflection/refraction at the inner walls of the microfluidic channel and in the liquid sample
Microfluidic channels
Plasmonic detection spots (SPR / LSPR)
Inlet
3.1. Experimental set-up for Au_NPs local synthesis
Laser
XYZ translation stage
Optical focusing system
Polychromatic readout light beam
Multichannel fiber spectrometer
J. Hastanin, C. Lenaerts, P. Gailly and K. Fleury-Frenette