## Slide 1
Influence of the microstructure and doping of CH3NH3PbI3 films as photoelectrodes in perovskite-based photovoltaic cells
N. Daem, J. Dewalque, G. Spronck, A. Schrijnemakers, R. Cloots, C. Henrist
<
Objective
Opal-like structuration: templating
Conclusion
Optoelectronics properties
The research was funded through the ARC grant for Concerted Research Actions, financed by the French Community of Belgium, and supported by the Walloon Region (SOLIDYE_1 Project, Complement FEDER, Grant agreement 1510607).
Acknowledgements
CH3NH3PbI3
inverse-opal photoanode
Photonic structure
Improvement of PV efficiency through photonic effect
Optimization of light interaction within the layer
Tuning of cell coloration/transparency
Two-steps deposition: (PS beads layer followed by perovskite precursor infiltration)
1) PS beads as structuring agent
2) Precursor solution infiltration and PS beads elimination
 CH3NH3PbI3 perovskite inverse-opal porous layer
Experimental settings:
PS beads suspension: 10 % vol.
in H2O/i-PrOH 50/50 vol.
PS beads diameter: 300 nm, 540 nm,
810 nm, 1000 nm or 2100 nm
Spin-coating parameters : 1000 RPM 30 s
Stabilisation: 70°C 30min
Perovskite
precursor
CH3NH3PbI3 precursor: PbI2 + MAI 0.7 M in DMSO
Spin-coating parameters: 2000RPM 30s
Stabilisation: 100°C 1h
Beads elimination: Toluene washing 2 min
Photovoltaic efficiency improvement with PS bead diameters
Photovoltaic efficiency improvement due to 3D structuration
Coloration of illuminated films on silicon substrates
Coloration and improvement with 3D structuration

Experimental settings:
0.1 %
1.0 %
1.1 %
1.9 %
0.8 %
2.3 %
PS beads
DENSE
PS 300
PS 540
PS 810
PS 1000
PS 2000
(%)
Dense
PS 810
PS 300
PS 540
PS 810
PS 1000
PS 2100
CH3NH3PbI3
dense photoanode
Dense