## Slide 1: Amélioration des performances des briques en terre comprimées à travers une réaction pouzzolanique
SustainEng2018: 12-14/12/2018, Ouagadougou-Burkina Faso
  NSHIMIYIMANA Philbert, MESSAN Adamah, COURARD Luc

## Slide 2
Compressed earth blocks for construction of modern housing
Notes: 1/3 of global population live in earth based housing
Healthy and comfortable in-door environnement

## Slide 3
Compressed earth blocks for construction of modern housing
Houben and Guillaud, 2006; Bogas et al. 2018
Traditional adobe bricks (1 MPa)
Modern compressed earth blocks (CEBs) (2 MPa)
Notes: 1/3 of global population live in earth based housing
Healthy and comfortable in-door environnement

## Slide 4
1. Cement: hydration reaction requires 28 days of curing.
2. Lime: pozzolanic reaction requiring >28 days of curing.
3. Geopolymer: geopolymerization of aluminosilicates by activation with alkaline solutions.
Chemical stabilization improves the performances of CEBs in saturated and dry conditions
Houben & Guillaud, 2006; Bogas et al. 2018; Al-Mukhtar et al. 2010, 2014; Sore et al. 2018

## Slide 5
Calcium carbide residue (CCR) and rice husk ash (RHA) for improving the performances of CEBs
Kinetic of reaction in solutions of mixtures :
Earth + CCR (calcium carbide residue)
Earth + CCR:RHA (rice husk ash)
2. Mechanical performances:
CEBs stabilized with CCR
CEBs stabilized with CCR:RHA
3. Mineral changes in cured mixtures.

## Slide 6
EXPERIMENTAL APPROACH

## Slide 7
Earthen material
Pulverized (<5 mm)
Kaolinite (>75 %)
CCR
Ball milled (<125 µm)
Active lime (50 %)
RHA
Calcinated : 500°C (2 h)
Ball milled (<80 µm)
Amorphous silica (70 %)
Raw materials were processed and characterized
Figure 3. Raw (top) and processed (bottom) materials

## Slide 8
Binder (CCR/CCR:RHA) was added to the earthen material on weight percentage basis
CCR | 0 | 5 | 8 | 10 | 15 | 20 | 25
CCR: RHA (ratios) | - | - | - | 10 | 15 | 20 | 25
 |  |  |  | (9:1) | (13.5:1.5) | (18:2) | (22.5:2.5)
 |  |  |  | (8:2) | (12:3) | (16:4) | (20:5)
 |  |  |  | (7:3) | (10.5:4.5) | (14:6) | (17.5:7.5)
 |  |  |  | (6:4) | (9:6) | (12:8) | (15:10)

## Slide 9
Mix solutions and CEBs were prepared, cured and characterized
  1. Curing mix solutions (1-90 days); 40±2°C
Concentration of free calcium [Ca2+]
Compressive strength in saturated and dry condition
Mineral change by XRD
  2. Prodution and Curing stabilized CEBs (45 days), 40±2 °C

## Slide 10
RESULTS & IMPLICATIONS

## Slide 11
Concentration of unconsumed calcium [Ca2+] in mix solutions reached the minimum after 45 days
Consumption of free [Ca2+] during the pozzolanic reaction
28
45
                Earth+20 % CCR:RHA(16:4)
Earth+20 % CCR

## Slide 12
CEBs stabilized with CCR/ CCR:RHA were resistant to the degradation after 2 hours in water
Pozzolanic reaction improved the cementation in CEBs
                Stabilized CEBs (5 % CCR)
Unstabilized CEBs (0 % CCR)

## Slide 13
Compressive strength of CEBs was improved and reached the maximum with 10-20 % CCR
Compressive strength required for load-bearing wall (4 MPa)
Dry
Saturated
Two-torey housing

## Slide 14
Compressive strength of CEBs was further improved with 20 % CCR:RHA in 16:4 ratio
RHA accelerated the pozzolanic reaction resulting in occurrence of extra compressive strength (6 MPa)
Dry
Saturated
Three-storey housing
Two-storey housing

## Slide 15
Cementitious products formed from the pozzolanic reaction between aluminosilicates and CCR
                CSH: Calcium Silicate Hydrate; CAH: Calcium Aluminate Hydrate K: kaolinite; P: Portlandite (active lime)

## Slide 16: CONCLUSIONS & REMARKS

## Slide 17
Conclusions and studies in perspective
Hydro-mechanical performances of CEBs were improved by stabilization with by-products :
  10-25 % CCR alone reaches 4 MPa required for two-storey housing;
  20 % CCR:RHA (16:4) reaches 6 MPa for tree-storey housing;
Investigate the performance of stabilized CEBs at early age;
Investigate the durability of CCR/CCR:RHA stabilized CEBs
Notes:   CCR alone requires at least 45 days for curing and reaching the 4 MPa for two-storey housing construction
  CCR:RHA requires 28 days for curing and imparting extra compressive strength for three-storey housing construction behaving more like cement

## Slide 18: MERCI POUR VOTRE ATTENTION
philbert.nshimiyimana@2ie-edu.org
pnshimiyimana@doct.uliege.be
Skype ID: philbert.nshimiyimana
PRD 2016-2021: Amélioration de la qualité de l’habitat en terre crue au Burkina Faso