## Slide 1: Recovery of Phosphorus from Sewage Sludge and Subsequent Purification Using Reactive Extraction
Shariff Z.A., Fraikin L., Léonard A., Pfennig A. za.shariff@uliege.be Products, Environment, and Processes (PEPs) Department of Chemical Engineering Université de Liège https://www.chemeng.uliege.be

## Slide 2: agenda
introduction
PULSE process concept
process development
  SLE modelling
  cascaded option tree
  experimental results
  summary

## Slide 3: introduction
Chart: 
essential element for all forms of life
finite resource
EU imports more than 90% of P
sewage has potential to cover more than 20% of P demand in North-West Europe
rock phosphate

## Slide 4: PULSE (Phosphorus University of Liege Sludge Extraction) process
acid
organic
solvent
base/Ca
drying
leaching
separation
reactive extraction
re-extraction
CaP/
solid
waste
metals
precipitation
dewatered
sludge
waste water
re-extraction agent/NH3
P + impurities

## Slide 5: modelling: SLE & speciation

## Slide 6: modelling tool: non-linear data fitting

## Slide 7: cascaded option tree: drying
P-recovery from sludge
drying conditions
- | dewatered sludge | 0 | 0 | 0 | - | 
+ | convective air drying | + | 0 | 0 | 0 | 0
 | slow drying (no air) | + |  | 0 | 0 | 0
extraction compatibility
filtrability
P leaching
operation cost
transport/handling/storage
- | not feasible
0 | acceptable
+ | good
 | not evaluated
Bednarz, A. et al. 2014
dried sludge
dewatered sludge

## Slide 8: P leaching with different acids and pH

## Slide 9: sludge leach liquor

## Slide 10: reactive extraction with HCl conc. 1mol/L

## Slide 11: reactive extraction of Fe with A336 + TBP
Alamine 336:
TBP:

## Slide 12: PULSE product
Component | Concentration
P2O5 | 29.2%
CaO | 21.7 %
Total C | 6 %
Al2O3 | 2.61 %
MgO | 1.84 %
Fe | 0.325 %
Mn | 10800ppm
Cr | 1530 ppm
Cu | 294 ppm
Ni | 51.6 ppm
Pb | 38,8 ppm
Zn | 8.97 ppm
Cd | 0.735ppm
Hg | 0.054 ppm
leaching of dried sludge
filtration
metal removal by reactive extraction
CaP precipitation with NaOH
(pH = 6 - 7)

## Slide 13: summary
no significant difference between P leaching from wet or dry sludge
P leaching depends only on pH and not on the type of acid
extraction of metals at low pH only achieved with Alamine 336
metals concentration in product is within the limits set by the EU fertilizer regulations except in case of Cr

## Slide 14: Acknowledegements
financing
  Interreg North-West Europe
  SPW-Wallonia
analytics
  Bogdan A. , Michels A., Meers E., Durand B. - Faculty of Bioscience Engineering, Ghent University, Belgium
  Kroonen D. & Baukens I. – Prayon S.A., Belgium

## Slide 15: Recovery of Phosphorus from Sewage Sludge and Subsequent Purification Using Reactive Extraction
Shariff Z.A., Fraikin L., Léonard A., Pfennig A. za.shariff@uliege.be Products, Environment, and Processes (PEPs) Department of Chemical Engineering Université de Liège https://www.chemeng.uliege.be

## Slide 16: References
http://www.nweurope.eu/projects/project-search/phos4you-phosphorus-recovery-from-waste-water-for-your-life/
Doetsch, P., Pinnekamp, Johannes, Montag, D., Rath, W., Grömping, M., 2010. Rückgewinnung von Pflanzennährstoffen, insbesondere Phosphor aus der Asche von Klärschlamm (Abschlussbericht PASCH). Institut für Siedlungswasserwirtschaft der RWTH Aachen, Aachen.
Bednarz, A., Rüngeler, B., Pfennig, A., 2014. Use of Cascaded Option Trees in Chemical-Engineering Process Development. Chem. Ing. Tech. 86, 611-620.