Supplementary Material

Carbon-Coated Porous TiO2 Layers Templated by Core-Shell Polymer Particles: Film Processing and Charge Transfer Resistance Assessment.

Vidhyadevi Thangaraj,a Jennifer Dewalque,b Anthony Maho,b Gilles Spronck,b Cédric Malherbe,c Abdelhafid Aqil,a Rudi Cloots,b Pierre Colson,b Christine Jérôme,a Antoine Debuignea*

a Center for Education and Research on Macromolecules (CERM), CESAM Research Unit, Chemistry Department, University of Liege (ULiege), Quartier Agora, 13 Allée du Six Août (Bldg B6a), Sart-Tilman, B-4000 Liège, Belgium.

b Group of Research in Energy and Environment from Materials (GREEnMat), CESAM Research Unit, Chemistry Department, University of Liege (ULiege), Quartier Agora, 13 Allée du Six Août (Bldg B6a), Sart-Tilman, B-4000 Liège, Belgium.

c Laboratory of Mass Spectrometry, Molsys Research Unit, Chemistry Department, University of Liege (ULiege), Quartier Agora, 13 Allée du Six Août (Bldg B6d), Sart-Tilman, B-4000 Liège, Belgium.

Figure S1. TGA curves recorded under nitrogen for the PS, PS-PAN and PS-PDA particles. Residual carbon of 0.33%, 3.97% and 4.07% are respectively determined for PS, PS-PAN and PS-PDA particles.

Figure S2. TEM image of the TiO2 film templated by PS-PAN particles, emphasizing the presence of a thin layer (~ 4 nm) of carbon at the surface of the TiO2 cavities.

Figure S3. X-ray diffractograms of the TiO2 porous films templated by PS-PDA and PS-PAN particles. The drop of intensity observed for the (101) TiO2 anatase peak at 25.3° on the TiO2/PS-PAN sample (in comparison with the TiO2/PS-PDA sample) is correlated to an amorphization of the corresponding TiO2 film. The presence of rutile is ruled out as the characteristic (110) TiO2 rutile peak at 27.4° is not observed.