## Slide 1: E-MRS
Antoine Merlo
01/06/2022
Environmental and economic assessment of advanced coatings over their whole life cycle: a case study on HiPIMS and TiAlN

## Slide 2: Introduction
Thin films are becoming more prevalent than ever
… and there is a need for environmental accountability!
Applying assessment techniques to deposition processes
Joint economic and environmental assessment
1

## Slide 3: PULSATEC project
INTERREG Great-Region project (Liège, NE France, West Germany, Luxembourg)
Project based around HiPIMS
High Powered Impulse Magnetron Sputtering!

## Slide 4: HiPIMS
Magnetron Sputtering: coating technology
Vaccuum chamber
Voltage to sputter target
HiPIMS: High V pulses to increase ionization rate!

## Slide 5: Characteristics of HiPIMS coatings
High energy  High density
More ions  Better coverage
Better adhesion
BUT lower deposition rate!

## Slide 6: Goal
HiPIMS: costlier, but better performing coatings than MS-DC
Evaluate costs and impacts for both:
  Coating phase
  Cutting phase
Higher tool life  Lower downtimes  Higher productivity and lower passive electricity consumption
Joint evaluation of costs and environmental impacts

## Slide 7: TiAlN and HiPIMS
Higher performances of HiPIMS coatings Improved tool life
Good enough to compensate higher HiPIMS costs?
Weichart, J. (2012). ‘Titanium aluminum nitride sputtered by HIPIMS’, IOP Conference Series Materials Science and Engineering

## Slide 8: Tools considered
HSS milling tools: 8mm diameter, 8 cm length
4µm TiAlN
Tool life of 75 min for HiPIMS and 50 min for MS-DC
1.8µm/h for HiPIMS 3.6µm/h for DC-MS

## Slide 9: Installations
200 tools per batch
Rotating and heating substrates
HiPIMS :1 300 000 € DC-MS :1 200 000 €
Same consumptions for both processes but longer deposition time for HiPIMS (133 min vs 67 min)

## Slide 10: Cost evaluation of 1 coating
Two 8h shifts per day (40€ per operator)
1464 vs 1094 batches a year (MS-DC vs HiPIMS)
0.08€/kWh
5 year payback
Chart: Cost per coating (€)
| HiPIMS | DC
Labor | 0.87778 | 0.65556
Consumables | 0.17058 | 0.11027
Annuities | 1.1887 | 0.81945
Maintenance | 0.11887 | 0.081945

## Slide 11: Environmental impact of 1 coating
CO2 emissions: 320.7 gCO2 for HiPIMS, 191.2 gCO2
Electricity production is the main factor (Belgian EF: 174 gCO2/kWh
Chart: CO2 emissions (g)
| HiPIMS | DC
Argon | 0.149 | 0.0975
Nitrogen | 0.0385 | 0.019
Target | 0.312 | 0.312
Electricity | 320.6915 | 191.1585

## Slide 12: Cutting phase
Inclusion of costs and impacts of cutting phase:
  Substrate
  Coatings
  Cutting fluid
  Electricity consumed
  Tool life has an impact on those factors!

## Slide 13: Cutting phase costs
Longer tool life leads to lower down times  Lower costs and higher productivity
Chart: Cost per machine piece (€)
| DC | HiPIMS
Operator | 28.39 | 26.49
Electricity | 0.046 | 0.045
Coating | 0.954 | 0.899
Tool | 3.43 | 2.28
Oil | 1.142 | 1.065

## Slide 14: Cutting phase impacts
Higher CO2 emissions for HiPIMS coatings, but:
  Less substrates used
  Less cutting fluid
  Less passive electricity usage
Chart: CO2 emissions per machine piece (g)
| DC | HiPIMS
Electricity | 99.67 | 96.35
Coating | 109.84 | 122.69
Tool | 317.35 | 211.57
Oil | 65.75 | 61.33
Oil disposal | 92.28 | 86.08

## Slide 15: Cutting phase evaluation conclusions
Use of HiPIMS reduces the total cost by around 10% and CO2 emissions by 15%
High potential for HiPIMS technology
Different operating parameters ?
  Lubrification conditions
  Cutting speed
Costa, Eder & Bacci Da Silva, Marcio & Machado, Alisson. (2009). Burr Produced on the Drilling Process as a Function of Tool Wear and Lubricant-Coolant Conditions. Journal of The Brazilian Society of Mechanical Sciences and Engineering - J BRAZ SOC MECH SCI ENG. 31. 10.1590/S1678-58782009000100009.

## Slide 16: Parametrisation: Taylor’s equation
Parametrisation of cost and CO2 (2 objectives)
 Use cutting speed as a parameter

## Slide 17: Parametrisation: Taylor’s equation
Until experimental data, assumed that tool lives and powers evolve with speed as in *
Chart: Cutting speed (m/min)
| 17.399999999999999 | 34.799999999999997 | 52.199999999999996 | 69.599999999999994 | 87
HiPIMS | 75 | 36 | 22.5 | 13.5 | 8.2
DC | 50 | 24 | 15 | 9 | 5.5
*Li, C. (2015). ‘A quantitative approach to analyze carbon emissions of CNC-based machining systems’, Journal of Intelligent Manufacturing 26, pp. 911-922

## Slide 18: Parametrisation
Plot of CO2 emissions vs costs
Several lubrication scenarios
Cutting speed varies between 5 and 100 m/min

## Slide 19: Parametrisation
Plot of CO2 emissions vs costs
Several lubrication scenarios
Cutting speed varies between 5 and 100 m/min
HiPIMS lowers both costs and CO2 impacts !

## Slide 20: Parametrisation
Plot of CO2 emissions vs costs
Several lubrication scenarios
Cutting speed varies between 5 and 100 m/min
HiPIMS lowers both costs and CO2 impacts !
Cutting speeds reduce costs, but increase CO2 emissions

## Slide 21: Parametrisation conclusions
HiPIMS in flood machining conditions seems to bring the best outcomes for both costs and CO2 emissions
Trade-offs between CO2 emissions and costs
How to choose the best cutting speed?
 Aggregation of CO2 emissions via a carbon tax

## Slide 22: Carbon tax: 120€/tCO2
Chart: Cutting speed (m/min)
| 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Base cost | 24 | 21 | 19.5 | 19 | 18 | 17 | 16.5 | 16
Carbon tax | 0.0678 | 0.06792 | 0.06852 | 0.06948 | 0.07044 | 0.07116 | 0.072 | 0.07296

## Slide 23: Carbon tax: 250€/tCO2
Chart: Cutting speed (m/min)
| 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Base cost | 24 | 21 | 19.5 | 19 | 18 | 17 | 16.5 | 16
Carbon tax | 0.14125 | 0.1415 | 0.14275 | 0.14475 | 0.14675 | 0.14825 | 0.15 | 0.152

## Slide 24: Carbon tax: 5000€/tCO2
Chart: Cutting speed (m/min)
| 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100
Base cost | 24 | 21 | 19.5 | 19 | 18 | 17 | 16.5 | 16
Carbon tax | 2.825 | 2.83 | 2.855 | 2.895 | 2.935 | 2.965 | 3 | 3.04

## Slide 25: TiAlN Conclusions
CO2 emissions differences are negligible, even with aberrant carbon taxes
HiPIMS in FM at high machining speeds seem to be the best option
Need of experimental data to validate assumptions

## Slide 26: Thank you for your attention!

## Slide 27: Références
[1] IndustryArc (2021). ‘Cutting Tools Market - Forecast(2021 - 2026)’
[2] Bobzin, K. (2016). ‘High-performance coatings for cutting tools’, CIRP Journal of Manufacturing Science and Technology
[3] Jindal, P.C. et al. (1999). ‘Performance of PVD TiN, TiCN, and TiAlN coated cemented carbide tools in turning’, International Journal of Refractory Metals & Hard Materials, 17, pp. 163-170.
[4] Kottfer, D. et al. (2013). ‘Investigation of Ti and Cr based PVD coatings deposited onto HSS Co 5 twist drills’, Applied Surface Science, 282, pp. 770-776.
[5] Münz, V.-D. (1986), ‘Titanium aluminum nitride films: A new alternative to TiN coatings’, Journal of Vacuum Science & Technology A, 4(6)
[6] Weichart, J. (2012). ‘Titanium aluminum nitride sputtered by HIPIMS’, IOP Conference Series Materials Science and Engineering
[7] Anders, A. (2010). ‘Deposition rates of high power impulse magnetron sputtering: Physics and economics’, Journal of Vacuum Science & Technology A 28, p. 783
[8] Li, C. (2015). ‘A quantitative approach to analyze carbon emissions of CNC-based machining systems’, Journal of Intelligent Manufacturing 26, pp. 911-922