## Slide 1
High Open-Circuit Voltage Lead-Free Cs2AgBiBr6 Double Perovskite Solar Cells from Spray-Coating Deposition
24th May 2022
València, HOPV 22
Nathan Daem
Nathan.Daem@uliege.be

## Slide 2
POWDERS
COATINGS
Hybrid and Inorganic Materials
with Controlled Micro- and Nanostructure
SUSPENSIONS
Applications for energy (batteries, smart windows, solar cells…), environment (recycling, air/water treatment, catalysis)
and health (additive manufacturing, biomaterials…)
ULiège- GREEnMat
Notes: For powders and coatings --> Pas from

## Slide 3
Alternative: lead free materials
Stability
Low toxicity
Cell processability
Photo
conversion efficiency
Notes: ATTENTION is one promising alternative
Eviter low efficiencies: are lower than the theoretical maximum efficiency

## Slide 4
Alternative: lead free materials
Stability
Low toxicity
Cell processability
Cs2AgBiBr6
A2MIMIIIX6
X= Br, Cl
A = monovalent cation
MI = monovalent metal ion
MIII = trivalent metal ion
Photo
conversion efficiency
Notes: ATTENTION is one promising alternative
Eviter low efficiencies: are lower than the theoretical maximum efficiency

## Slide 5
Alternative: lead free materials
Stability
Low toxicity
Cell processability
Cs2AgBiBr6
A2MIMIIIX6
X= Br, Cl
A = monovalent cation
MI = monovalent metal ion
MIII = trivalent metal ion
Photo
conversion efficiency
Notes: ATTENTION is one promising alternative
Eviter low efficiencies: are lower than the theoretical maximum efficiency

## Slide 6
Strategy
Deposition of double perovskite (Cs2AgBiBr6) layers by spin-coating and ultrasonic spray pyrolysis (USP)
Solution of precursors
TiO2
Solution of precursors
Ultrasonic generator
Carrier gas
TiO2
Lab scale
(Spin coating)
Scalable process
(USP)
vs.
Notes: Aspect fondamental: comparaison des 2 méthodes (morphologie, paramètres etc.) pas juste upscaling
Parler de l’ExactaCoat (permet de déposer jusqu’à 40X40cm)
ATTENTION ne pas citer tous les paramètres de dépôts USP
Méchanismes de dépôts différents donc comparaison fondamentale des deux techniques (spin: référence et USP et peut être développé pour des plus grandes surfaces).

## Slide 7
Cs2AgBiBr6 solar cell architecture
Substrate
FTO conducting glass
Notes: The most appropriate architecture (n-i-p)
Pas préciser les épaisseurs

## Slide 8
Cs2AgBiBr6 solar cell architecture
Substrate
FTO conducting glass
Dense TiO2
Avoids short-cuts
Notes: The most appropriate architecture (n-i-p)
Pas préciser les épaisseurs

## Slide 9
Cs2AgBiBr6 solar cell architecture
Mesoporous TiO2
Filled with Cs2AgBiBr6
Collects electrons
Substrate
FTO conducting glass
Dense TiO2
Avoids short-cuts
Notes: The most appropriate architecture (n-i-p)
Pas préciser les épaisseurs

## Slide 10
Cs2AgBiBr6 solar cell architecture
Mesoporous TiO2
Filled with Cs2AgBiBr6
Collects electrons
Double perovskite
Cs2AgBiBr6
Absorbs light, creates electron-hole pairs
Substrate
FTO conducting glass
Dense TiO2
Avoids short-cuts
Notes: The most appropriate architecture (n-i-p)
Pas préciser les épaisseurs

## Slide 11
Cs2AgBiBr6 solar cell architecture
Mesoporous TiO2
Filled with Cs2AgBiBr6
Collects electrons
Double perovskite
Cs2AgBiBr6
Absorbs light, creates electron-hole pairs
Substrate
FTO conducting glass
Dense TiO2
Avoids short-cuts
Hole transporting material
Spiro-OMeTAD
Notes: The most appropriate architecture (n-i-p)
Pas préciser les épaisseurs

## Slide 12
Cs2AgBiBr6 solar cell architecture
Mesoporous TiO2
Filled with Cs2AgBiBr6
Collects electrons
Double perovskite
Cs2AgBiBr6
Absorbs light, creates electron-hole pairs
Substrate
FTO conducting glass
Dense TiO2
Avoids short-cuts
Hole transporting material
Spiro-OMeTAD
Counter-electrode
Gold
Notes: The most appropriate architecture (n-i-p)
Pas préciser les épaisseurs

## Slide 13
Cs2AgBiBr6 solar cell architecture
Mesoporous TiO2
Filled with Cs2AgBiBr6
Collects electrons
Double perovskite
Cs2AgBiBr6
Absorbs light, creates electron-hole pairs
Substrate
FTO conducting glass
Dense TiO2
Avoids short-cuts
Hole transporting material
Spiro-OMeTAD
Counter-electrode
Gold
Spin VS USP
Notes: The most appropriate architecture (n-i-p)
Pas préciser les épaisseurs

## Slide 14
Publication

## Slide 15
Morphology-SEM
Spin-coated double perovskite film
Top view
Cross section
(film + solar cell)
Spray-coated double perovskite film
Top view
Cross section
(film + solar cell)

## Slide 16
Morphology-SEM
Spin-coated double perovskite film
Top view
Cross section
(film + solar cell)
Spray-coated double perovskite film
Top view
Spray: higher coverage and smaller grains (150 nm VS 350 nm)
Spin/Spray: overlayer = 150-200 nm
Cross section
(film + solar cell)

## Slide 17
Structure-XRD
Spray-coated film
Spin-coated film
Reference
(VESTA simulated)
: Cs2AgBiBr6
No impurities
Crystallite size similar: 35 nm

## Slide 18
Optical properties-UV-VIS
Spray-coated film
Spin-coated film
Spin-coated: Eg 2.25 eV (direct bandgap)
Spray-coated: Eg 2.15 eV (direct bandgap)
2
1
5
.
1
5
.
0

## Slide 19
Optical properties-UV-VIS
Spray-coated film
Spin-coated film
Spin-coated: Eg 2.25 eV (direct bandgap)
Spray-coated: Eg 2.15 eV (direct bandgap)
Higher absorbance for spray-coated film compared with spin-coated:
Different values of Eg for Cs2AgBiBr6 films due to different preparation methods
2
1
5
.
1
5
.
0

## Slide 20
Optoelectronic properties-Photoluminescence
Prof. Samuel D. Stranks
Notes: identify collab. U Cambridge (photo Sam) + parameters of PL measurements ; also PL mapping explanation (quite unique)
The higher the peak is, the better the photovoltaic compound is (longer electron lifetime).

## Slide 21
Spray-coated film
Spin-coated film
Maximum of the curves at the same wavelength (640 nm ≈ 1.9 eV)  indirect bandgap
Higher PL intensity for spray VS spin (higher absorption and less recombination)
 Spray: very promising in terms of optoelectronic properties
Optoelectronic properties-Photoluminescence
Prof. Samuel D. Stranks
Notes: identify collab. U Cambridge (photo Sam) + parameters of PL measurements ; also PL mapping explanation (quite unique)
Faire animations: trop chargé
The higher the peak is, the better the photovoltaic compound is (longer electron lifetime).

## Slide 22
Photovoltaic properties-I-V curves
Spray-coated film
Spin-coated film
 |  | Voc (V) | Jsc (mA/cm2) | FF | PCE (%)
Spin-coated device | Direct | 0.827 | 3.6 | 81 | 2.3
 | Reverse | 0.811 | 3.7 | 78 | 2.3
Spray-coated device | Direct | 1.091 | 3.1 | 70 | 2.3
 | Reverse | 1.093 | 3.2 | 68 | 2.3
Notes: Despite the higher absorbance and the better connectivity the spray-coated device shows reduced current density (Jsc) compared with the spin-coated benchmark and this trend is corroborated by the external quantum efficiency (EQE) measurements.
To further analyze the charge transfer properties of spin- coated and spray-coated Cs2AgBiBr6-based solar cells electrochemical impedance spectroscopy (EIS) is conducted.
Dire que c’est ma cellule championne
Uniformiser tableau

## Slide 23
Photovoltaic properties-I-V curves
Spray-coated film
Spin-coated film
 |  | Voc (V) | Jsc (mA/cm2) | FF | PCE (%)
Spin-coated device | Direct | 0.827 | 3.6 | 81 | 2.3
 | Reverse | 0.811 | 3.7 | 78 | 2.3
Spray-coated device | Direct | 1.091 | 3.1 | 70 | 2.3
 | Reverse | 1.093 | 3.2 | 68 | 2.3
Among the highest efficiencies reached to date (2.3% vs. 2.5%)
Spray: no hysteresis and higher Voc (cf PL)
BUT lower Jsc  Why?
Notes: Despite the higher absorbance and the better connectivity the spray-coated device shows reduced current density (Jsc) compared with the spin-coated benchmark and this trend is corroborated by the external quantum efficiency (EQE) measurements.
To further analyze the charge transfer properties of spin- coated and spray-coated Cs2AgBiBr6-based solar cells electrochemical impedance spectroscopy (EIS) is conducted.
Dire que c’est ma cellule championne
Uniformiser tableau

## Slide 24
Photovoltaic properties- EIS
 | R1 [Ω] | Q2 [10−6 F. sa−1] | a | R2 [Ω] | Q3 [10−6 F.sb−1] | b | R3 [Ω]
Spin-coated device | 10 | 0.381 | 0.979 | 178 | 0.615 | 0.808 | 254
Spray-coated device | 11 | 0.235 | 0.850 | 191 | 0.831 | 0.806 | 367
Recombination at the Cs2AgBiBr6/Spiro interface: R3 ↑ = recombination ↓
 Spray: lower recombination rate (VOC ↑)
Notes: Data were fitted with the equivalent circuit model.The equivalent electrical circuit consists of: an R1 resistance associated with wires and contacts; an R2//Q2 element characteristic of the selective contacts, including c-TiO2 and mp-TiO2 for electron-selective contacts and the Spiro-OMeTAD for hole-selective contacts, respectively and an R3//Q3 element for interfacial recombination between electrons and holes
Focus on two parameters: R3 and R2
EIS data corroborate PL and J–V results

## Slide 25
Photovoltaic properties- EIS
 | R1 [Ω] | Q2 [10−6 F. sa−1] | a | R2 [Ω] | Q3 [10−6 F.sb−1] | b | R3 [Ω]
Spin-coated device | 10 | 0.381 | 0.979 | 178 | 0.615 | 0.808 | 254
Spray-coated device | 11 | 0.235 | 0.850 | 191 | 0.831 | 0.806 | 367
Selective contact resistance:
Spray: R2 ↑ = less efficient charge transfer
With Spin: larger grains and better infilitration
Notes: Data were fitted with the equivalent circuit model.The equivalent electrical circuit consists of: an R1 resistance associated with wires and contacts; an R2//Q2 element characteristic of the selective contacts, including c-TiO2 and mp-TiO2 for electron-selective contacts and the Spiro-OMeTAD for hole-selective contacts, respectively and an R3//Q3 element for interfacial recombination between electrons and holes
Focus on two parameters: R3 and R2
EIS data corroborate PL and J–V results

## Slide 26
Conclusion
A2MIMIIIX6
X= Br, Cl
A = monovalent cation
MI = monovalent metal ion
MIII = trivalent metal ion
Cs2AgBiBr6
Easy processability
High stability
Nontoxicity
Notes: Perspectives : facilitate infiltration, substitution, improve hole conduction => PEN/TET
To conclude about Cs2AgBiBr6 as an alternative lead-free perovskite

## Slide 27
Conclusion
A2MIMIIIX6
X= Br, Cl
A = monovalent cation
MI = monovalent metal ion
MIII = trivalent metal ion
Cs2AgBiBr6
Easy processability
High stability
Nontoxicity
Spray-coating
Smooth and uniform film
Smaller and better
connected grains
PCE: 2.3 % (Voc )
Notes: Perspectives : facilitate infiltration, substitution, improve hole conduction => PEN/TET
To conclude about Cs2AgBiBr6 as an alternative lead-free perovskite

## Slide 28
Conclusion
A2MIMIIIX6
X= Br, Cl
A = monovalent cation
MI = monovalent metal ion
MIII = trivalent metal ion
Cs2AgBiBr6
Easy processability
High stability
Nontoxicity
Spray-coating
Next steps
Efficiencies improvement by
Substitution of elements
Improvement of Cs2AgBiBr6/Spiro interface
Smooth and uniform film
Smaller and better
connected grains
PCE: 2.3 % (Voc )
Notes: Perspectives : facilitate infiltration, substitution, improve hole conduction => PEN/TET
To conclude about Cs2AgBiBr6 as an alternative lead-free perovskite

## Slide 29
Funding: University of Liège and FNRS
University of Liège – GREEnMat
  Prof. Rudi Cloots
  Dr. Pierre Colson
  Dr. Anthony Maho
  Dr. Jennifer Dewalque
  Gilles Spronck
  ULiège-GREENMAT co-workers & collaborators
University of Cambridge
  Prof. Samuel D. Stranks
  Dr. Felix Lang
  Stranks’ Lab co-workers & collaborators
Acknowledgements

## Slide 30
Website : http://www.greenmat.uliege.be
E-mail: nathan.daem@uliege.be
Thank you for
your attention
15

## Slide 31
Ultrasonic spray pyrolysis
Notes: Atomization with US => micron-sized droplets sprayed onto glass surface

## Slide 32
Perspectives- Stability tests
Tests recommandés (Normes ISOS-1) | 
Storage in humidity | Temperature= RT/65 °C
 | RH= dessiccator (20%)/ no controlled
Prolonged illumination test | Temperature= RT
 | RH= room humidity
Test of cycle illumination-humidity-thermal treatment | Temperature= RT RH: no controlled
M. V. Khenkin et al., “Consensus statement for stability assessment and reporting for perovskite photovoltaics based on ISOS procedures,” Nat. Energy, vol. 5, no. 1, pp. 35–49, 2020
1st tests: essential encapsulation for the rest of study: cover glass, thermoplastic, epoxy resin

## Slide 33
@ 70°C
+
@ 150°C
CsBr, AgBr, BiBr3 in DMSO
CsBr, AgBr, BiBr3 in DMF:DMSO
Spin-coating
Ultrasonic spray pyrolisis
@ 70°C
Strategy- double perovskite focus
18