## Slide 1: Architectured Interfaces in Bimaterial Attachements

## Slide 2
Bimaterial Attachments In Nature
Achilles tendon
Locke et al., ACS Biomaterials 2016
Dunlop at al., Materials Today 2011
Long gradient
Short gradient
E 20 GPa
E0.5 GPa
500µm
Rossetti et al, Nat Mat 2017
OR
Deformability
Stiffness
Side attached
to soft body
Side attached to hard surface
E ~ 0.2 MPa
E ~ 25 GPa
cm

## Slide 3
Bimaterial Interfaces with 3D Printing Technology
Stratasys Objet260 Connex2 :
Droplets dimension : 40 µm
Control on local microstructure and mechanical properties
High geometrical freedom
Allows Voxel 3D printing
Voxel 3D printing

## Slide 4
Interfaces in Polyjet Printing as Weak Regions
Printing direction
Material properties
Adapted from Lumpe et al., Materials and Design 2019
Interface as weakness :
Results
Printing direction (y)
Elastic contrast should not be too high
ERigid
ESoft
Stiffness ratio =

## Slide 5
Interface as weakness :
Intermediate layer reduces stress mismatch
Optimised Young’s Modulus is
Interfaces in Polyjet Printing as Weak Regions
A.Y. Uzan, O. Milo, Y. Politi et al., Principles of elastic bridging in biological materials, Acta Biomaterialia

## Slide 6
Aims
Prototype new bimaterial attachments based on minimal perturbation using voxel 3D printing
Aim 1 :
Understand impact of perturbations on stiffness, strength, failure behaviour
Aim 2 :
Understand local stress distribution at interfaces
Aim 3 :

## Slide 7
Methodology
Droplets mix
Voxel size chosen is 420x420 µm²
Types of bimaterial attachments :
Minimal perturbation : < 10% length
Flat interface (Reference case)
Ordered Interface patterning (6 configurations)
Methods :
Voxel based finite element simulations
Experimental testing on 3D printed bimaterial samples
Zorzetto et al., Scientific Reports 2020

## Slide 8
Methodology
Ordered:
Soft
(E = 50 MPa)
Rigid
(E = 2 GPa)
Softer layer
(E = 2 MPa)
Flat
Triangular
Chessboard
Rectangular
Interlocking
Soft interface
Staggered
Only 4 voxels perturbation

## Slide 9
Results : Flat & Soft
Soft intermediate layer decreases the stress mismatch
Flat
Soft interface

## Slide 10
Results : Flat & Soft
Soft intermediate layer decrease the stress mismatch
Flat
Soft interface

## Slide 11
Results : Other geometries
Digitation
Flat
Chessboard

## Slide 12
Triangular
Staggered
Interlocking
Results : Other geometries

## Slide 13
Results : Distance of the max Stress from free edge
Maximum of Stress is taken away from free edge
Does it delay breaking of samples ?
    See experimental results
D

## Slide 14
Results : Effect of width : Soft interface 2MPa
4 voxels
8 voxels
16 voxels
32 voxels
4 voxels = 1.68mm
8 voxels = 3.36mm
16 voxels = 6.72mm
32 voxels = 13.44mm

## Slide 15
Results : Reduce mismatch with Soft interface
Minimisation of mismatch criteria met ! Optimised Young’s Modulus is
Soft Interface Optimised (316 MPa) 32 voxels wide
Soft Interface 500 MPa
32 voxels wide
Soft Interface 2MPa
32 voxels wide

## Slide 16
Results : Reduce mismatch with Soft interface
Minimisation of mismatch criteria is not met when the layer is too small
Soft Interface Optimsed (316 Mpa)
Soft Interface 500 MPa
Soft Interface 2 MPa

## Slide 17
Results : Stress-strain
Fractured samples

## Slide 18
Results : Stress-strain
Fractured samples

## Slide 19
Results : Stress-strain
Fractured samples

## Slide 20
Results : Stress-strain
Fractured samples

## Slide 21
Results : Stress-strain
Fractured samples

## Slide 22
Results : Stress-strain
Fractured samples

## Slide 23
Results : Apparent Stiffness & Strength
Strength increases significantly while apparent stiffness stays approximately constant

## Slide 24
Results : Work Pre/Post-Failure
Post-failure work
Pre-failure work
Max increase : pre-failure work 3x
post-failure work 5x
Ordered
Displacement
Force

## Slide 25
Conclusions
Adding a small layer of soft materials decreases the stress mismatch between materials.
      Towards increased fatigue performance ?
Minimal perturbations increase strength and failure resistance of bimaterial attachment.
Interface patterning induces a shift in the maximum stress inside the bulk of material.
      Increased mechanical properties in uniaxial tension !

## Slide 26: Architectured Interfaces in Bimaterial Attachements
Quentin Grossman
Mechanics of Biological and
Bioinspired Materials Laboratory
Davide Ruffoni
Peter Varga
Belgium

## Slide 27
Results : Other geometries
Flat
Digitation
Chessboard
Staggered
Interlocking
Triangular

## Slide 28
Von Mises Stress Distribution
Mean VM
Distribution
[MPa]
Std VM
Triangular
Staggered
75% VF
Flat
Triangular
75% VF
Flat
Staggered
Stress concentration is taken away from edges
Spread of Stress : Higher amount of voxels with high and low Stress