## Slide 1
📅 16/11/2023
✉ Astrid.Cantamessa@uliege.be
🌐 www.biomat.uliege.be
MINERALIZATION AND MECHANICAL INSIGHTS OF CEMENT LINES IN HUMAN OSTEONAL BONE
A Cantamessa 1, S Blouin 2, S Amini ³, M Rummler ³, A Berzlanovich 4, R Weinkamer ³, MA Hartmann 2, D Ruffoni 1
1 University of Liege, Liege, Belgium ;
2 Ludwig Boltzmann Institute of Osteology, Vienna, Austria ;
³ Max Planck Institute of Colloids and Interfaces, Potsdam, Germany ;
4 Center of Forensics Medicine, Vienna, Austria.
Annual Meeting of the IEEE-EMB Benelux Chapter

## Slide 2: What are cement lines (CLs)?
1/14
CL: thickness = 1–3 µm
30 µm
50 µm
Roschger et al., Bone, 2008
Notes: As you might know, bone is highly heterogeneous. At the milimeter length scale, bone is either organized in the high-density type of cortical (or compact) bone, forming the wall of long bones or in the highly porous type of trabecular (or cancellous) bone located at the end of those long bones. Due to the biological processes of bone remodeling and mineralization, both types of bone are highly heteregenous and composed of different bone structure units. In human cortical bone, the main units are the osteons, which are specialized structure surrounding a large blood vessel, whereas in trabecular bone, the basic structural units are bone packets. Cement lines are the tiny interfaces bonding those units together and separating newly formed bone from older bone. In this work, we will only focus on cortical bone samples.

## Slide 3: What are the unknowns about cement lines (CLs)?
2/14
CL
Mineralization/Time [year]
Adapted from Roschger et al., Acta Biomater., 2020
Old bone
New bone
Formation of secondary osteons
Osteoclasts
 Resorbing bone
Osteoblasts
 Forming lamellae
Precursors of osteoblasts
 Forming CL
Remodeling cone
CL
Mineralization kinetics
Low mineralization
High mineralization
Notes: Going back to the beginning, CLs are formed during the remodeling process and the formation of secondary osteons which is happening as follows:
First, the osteoclasts are resorbing old bone releasing ions of minerals but little is known about what is happening to this mineral afterwards.
Then, CL are probably deposited first quite fast by precursors of osteoblasts.
Finally, osteoblasts are depositing new unmineralized bone more slowly.
Newly deposited bone is initially mineral-free and the mineral content (and hence the stiffness) increases with time in both new bone and CLs. However, there is not a lot of information about CL mineralization kinetic compared to the one of osteonal bone.
There are still lots of uncertainties about CL formation and mineralization and this is the reason why we will focus not only on the CL but aslo on its neighborhood as reference.

## Slide 4: Why studying cement lines (CLs)?
3/14
Computational studies
Giner et al., Engineering Fracture Mechanics, 2017
CLs are believed to interact with cracks
= Protective role
Experimental studies
Research questions:
Composition
Structure
Mechanical properties
Outcomes:
Better predictions of bone fracture
Better understanding of bone remodeling
New bioinspired composites
Notes: It has been observed from experimental studies that cracks were often stopped or deflected by CL. Computationnally, similar phenomena have been studied. We believe that CL are protecting osteons by interacting with cracks.
Despite their recognized importances, CL remains a poorly understood structure of our bones. Specifically, their composition, mineral properties, and biomechanical behavior are understudied. Studying the CLs could improve our knowledge on bone fragility and our ability to assess the fracture risk. It could also provide essential data for improving models or simulations of bone fracture and bone remodeling, which are just assuming CLs properties until now. Finally, it could also help to develop new bioinspired composites for many other applications.

## Slide 5: Aims & techniques
 Characterization of mineral content and mechanical properties of CL and its surroundings
Mineral content: Is there a relationship between the mineral content of CL and of surrounding bone?
Mechanical properties: Is CL stiffer or more compliant than corresponding osteonal bone?
▼ nIND (4)
Lateral spacing: 1 µm
Human femoral bone
2 samples (males, 40 & 81 y.o.)
35 uninterrupted osteons
4/14
🔬 qBEI (1)
Pixel size: 570 nm
🔬 hrBEI (3)
Pixel size: 75 nm
10 µm
50 µm
🔬 SHG (2)
Pixel size: 380 nm
(1) Quantitative backscattered electron imaging
(3) High resolution backscattered electron imaging
(2) Second harmonic generation
(4) Nanoindentation
50 µm
Notes: In this research, we characterize the mineral content and mechanical properties of CL and its surroundings. We prepare samples from two human femurs from which we select 35 uninterrupted (or full, latest deposited) osteons to study.
For the mineral content part, we explore the relationship between the mineral content of CL and of the surrounding bone tissue. We perform 2 techniques on the same locations: First, quantitative backscattered electron imaging to quantify the mineral content. Then, second harmonic generation to better see the lamellae and to classify the osteons as whether there are full/uninterrupted or not.
For the mechanical properties, we want to know if the CLs are stiffer or more compliant than their corresponding osteon. To do so, we use local nanoindentation to obtain the modulus and hardness. Then, high resolution backscattered electron imaging post-nanoindentation to see the indents and be able to correlate with the mineral content.
But first, let’s focus on the mineral content analysis.
 Assumption: The formation of CL may not require substantial mineral transport as in the case of osteonal bone [Raguin, Advanced Sciences, 2023]

## Slide 6: Methods | Layers segmentation & data post-processing
5/14
🔬 qBEI
Pixel size: 570 nm
Layer analysis [2 pix ≃1 µm]
Frequency distribution of Ca content in each layer
From layers to sectors
30 µm
30 µm
Layer outside 3 (O3)
Layer outside 2 (O2)
Layer outside 1 (O1)
Layer inside 3 (I3)
Layer inside 2 (I2)
Layer inside 1 (I1)
Cement Line (CL)
Average Osteon (Os)
Global analysis
Local analysis
Ca [wt %]
30
26
22
Notes: From qBEI images, CLs appear brighter so we can manually segment them. Then, we want to compare to other layers so we extract the two first layers inside, which were deposited just after the CL. We also segment a layer 20 pixels more inside as reference for the osteon. Finally, we extract the corresponding 3 layers outside, deposited before, to know if this is influencing the CL.
Then, we start with a global analysis by performing frequency distributions of Ca content of each layer.
Finally, for a more local analysis, we divide each layer into 16 sectors and average the Ca content within those sectors. We represent those results in polar plot.
20-40 µm/day
1-1.5 µm in depth

## Slide 7
CL higher mineral content
Mineral content of CL follows outer layers polar profile
CL higher mineral content
6/14
Results | Analysis of a low mineralized ‘young’ osteon
I1
CL O1 O2 O3
I2
I3
Global analysis
O3
O2
O1
I3
I2
I1
CL
Os
Ca mean =
21.79 wt %
‘Younger’
Local analysis
Ca [wt %]
50 µm
50 µm
10 µm
20
24
28
Notes: Here is a first example for a low mineralized osteon, a young one, on which all layers are represented in this picture. From SHG, we can observe that lamellae are no visible so we can classify this osteon as dark osteon according to the literature. For the global analysis, from the frequency distribution, we see two distinct peaks for the inside and the outside environment and CL has a higher mineral content than the osteon, quite close to the one of the outside. This peak at the CL is even more visible in this profile plot of the mineral content across each layer. Now, more locally, we can observe that the CL is quite interestingly following the outer layers polar profile, especially the first layers, even though there were not deposited at the same time. By contrast, there is no correlation between the Ca content of CL and the inside environment although there were deposited nearly at the same time.

## Slide 8
CL higher mineral content
Mineral content of CL follows much less outer layers polar profile
7/14
Results | Analysis of a high mineralized ‘old’ osteon
CL higher mineral content
‘Older’
Local analysis
O3
O2
O1
I3
I2
I1
CL
Os
I1
CL O1 O2 O3
I2
I3
50 µm
50 µm
10 µm
Global analysis
Ca mean =
26.4 wt %
Ca [wt %]
22
26
30
Notes: Now for a high mineralized osteon, or old osteon. This time, we clearly see the lamellae on SHG image so this is a bright osteon. From the frequency distributions, the two peaks are much less distinct but the CL has clearly still a higher mineral content. Also relfected in the profile plot. Now, in the local analysis, we see that this time the CL is not following the outside nor the inside.

## Slide 9: Results | Analysis of the whole set of osteons
Out
In
I3 I2 I1 CL O1 O2 O3
8/14
 CL ~10% more mineralized than corresponding osteon
Out
In
I3 I2 I1 CL O1 O2 O3
O3
O2
O1
I3
I2
I1
CL
Os
35 osteons
Notes: Those two examples were the extreme cases in terms of low and high mineralized osteon. However, looking now at all osteons, the tendency of higher mineral content for the CL, the tendency is confirmed. CL is approximately 10% more mineralized than its corresponding osteon

## Slide 10: Results | Impact of surrounding bone
Ca [wt %]
24
26
28
30
R² = 0.21
p <0.05
24
26
28
30
R² = 0.41
p <0.05
24
26
28
30
R² = 0.78
p <0.05
Ca [wt %]
Ca [wt %]
R² = 0.36
p <0.05
24
26
28
30
9/14
O1
I1
CL
Os
Osteon Ca [wt %]
Strong correlation between Ca content of CL and outside environment
‘Younger’
‘Older’
Ca [wt %]
Ca [wt %]
20
24
28
Ca [wt %]
22
26
30
35 osteons
Notes: Now, looking more locally and based on our previous observations that CL polar profile followed the one of the outside for young osteons, we represent the correlation between the Ca content of the outside and of the CL for different level of osteon mineralization. For young osteon, this correlation is strong, the outside envrionment is clearly influencing the composition of the CL. Then, this correlation decreases with time but increases again for the oldest osteons, probably due to a state of saturation for both older bone and CL.

## Slide 11: Aims & techniques
 Characterization of mineral content and mechanical properties of CL and its surroundings
Mineral content: Is there a relationship between the mineral content of CL and of surrounding bone?
Mechanical properties: Is CL stiffer or more compliant than corresponding osteonal bone?
▼ nIND (4)
Lateral spacing: 1 µm
Human femoral bone
2 samples (40 & 81 y.o.)
35 uninterrupted osteons
10/14
🔬 qBEI (1)
Pixel size: 570 nm
🔬 hrBEI (3)
Pixel size: 75 nm
10 µm
50 µm
🔬 SHG (2)
Pixel size: 380 nm
(1) Quantitative backscattered electron imaging
(3) High resolution backscattered electron imaging
(2) Second harmonic generation
(4) Nanoindentation
50 µm

## Slide 12
3 µm
11/14
🔬 hrBEI
Pixel size: 75 nm
▼ nIND
Lateral spacing: 1 µm
Applied force: 500 µN
Penetration depth: ~150 nm
🔬 hrSEI
Pixel size: 75 nm
500 µN
150 nN
20 25 30
Er [GPa]
Methods | Nanoindentation & data processing
CL
Notes: We perform some grids of indents with a load of 500 µN. We make a compromise to obtain a low lateral spacing for a better resolution while still having deep enough indents to avoid feeling the roughness. Then, we use high resolution second electron imaging post nanoindentation to detect indents. However, with this technique we don’t see the CL so we also use backscattered electron imaging with the same resolution that we overlap to see which indents are falling within the CL. Here is the final 2D map of the modulus in this region.

## Slide 13
Periodic alternation of:
  - Stiffer (22.98 ± 2.71 GPa) lamellae
  - Softer (20.69 ± 2.05 GPa) lamellae
Distinct peak for CL (26.45 ± 1.31 GPa) compared to corresponding osteon (p <0.01)
21 19 17 13 9 6 4 1 0 -3
Os
3 µm
12/14
20
25
30
Er [GPa]
3 µm
Os1
Os2
Os1
General analysis of the mechanical properties
3 µm
Os2
CL
Distance from CL [µm]
21 19 17 13 9 6 4 1 0
Periodic alternation of:
  - Stiffer (22.98 ± 2.71 GPa) lamellae
  - Softer (20.69 ± 2.05 GPa) lamellae
50 µm
50 µm
Notes: Here is an example of a typical grid that we perform within this small square. From SGH, we see that there is no signal coming form CL meaning that either fibers are out of plane or more random but we do not know. The corresponding 2D map shows an alternation of stiffer and softer layers (more than 10% diff) corresponding to bone lamellae. We also see the CL which more than 15% stiffer than its corresponding osteon. Indeed, when now looking at the older osteon, its stiffness is higher, probably because it was formed before. Hardness results are not represented here because they show the same tendency than the modulus. Those results were also confirmed in all grids we perform.
Same tendency with hardness
More than 10% diff between stiff and soft lamellae
CL >15% stiffer (17%) than corresponding osteon

## Slide 14
13/14
Mineral Content:
CL hypermineralized
Strong correlation between mineral content of CL and outside environment within young osteon
Local recycling of minerals already there to build new CL
Mechanical Properties:
CL stiffer than its corresponding osteon
 Consistent with reduced nanoporosity of CL [4]
 Hamper crack propagation
Image from simulation of T. Volders @MBBM lab, ULiège
 Consistent with [1]
Conclusions & perspectives
 In contradictions with softer CL [2,3]
[1] Roschger et al., Acta Biomater., 2020
[2] Zhou et al., EMI, 2020
[3] Montalbano et al., J. Mater. Res., 2011
[4] Tang et al., JBMR, 2023
Perspectives:
CL mineral properties measured with X-ray scattering @ESRF
Interplay between CL and osteocyte lacuno-canalicular network
4.5
4
3.5
3
2.5
2
Mineral particle thickness [nm]
CLS
SRµCT
Notes: To conclude, we observe that CL present a higher mineral content. There is also a strong correlation between the mineral content of CL and its outside envrionment within young osteon. Those two findings could suggest a local recycling of minerals already there and relased by osteoclasts when they were eating aways older bone to build to the new CL. This possible explanation was already previously suggested for osteonal bone in a paper comparing bone mineralization during modeling and remodeling.
We also find that CL are stiffer than their corresponding osteon. This difference of mechanical properties is hampering crack from entering inside the osteons as it was already observed.
Both findings are in agreement with the latest discovery of a nanochannel network within bone which is quite reduced at the CL. Less porosity meaning more bone per voxels could suggests higher mineral content and higher stiffness.
We will continue this work by additional exploration of the mineral properties that we already measured with x-ray scattering at the ESRF in Grenoble. We just need to process everything. Moreover, we will analyse the interplay between the CL and osteocyte lacuno-canalicular network.

## Slide 15
Mechanics of Biological and Bioinspired Materials laboratory
University of Liege, Belgium
14/14
Astrid
CANTAMESSA
Davide RUFFONI
Richard WEINKAMER
Maximilian RUMMLER
Shahrouz AMINI
Stéphane BLOUIN
Markus
HARTMANN
Andrea
BERZLANOVICH
Thanks to all co-authors

## Slide 16
Thank you for your attention!
Astrid Cantamessa
@astrid_canta

## Slide 17
Spatial correlation between periodic variations in stiffness (p < 0.01) and in mineral content (p < 0.01)
Peaks of mineral content and stiffness at CL
20
25
4
A
B
30
25
20
Er [GPa]
3 µm
A
B
Ca [wt %]
16
20
24
28
30
26
22
18
14
3 µm
CL
CL
A
B
Correlation of mineral content & mechanical properties
Notes: Now, we correlate mechanical properties and mineral content from qBEI and we plot both profiles along 2 lines. We clearly see a spatial correlation between the periodic variations in stiffness and mineral content corresponding to the alternation of lamellae. Moreover, we see peaks of both mineral content and stiffness at the CL location.

## Slide 18: Results | Kinetics analysis
‘Time’
R² = 0.57
P <0.05
Correlation between Ca content of CL and osteon
Different mineralization kinetics
Milovanovic et al., Bone, 2018
R² = 1
CL
Os
Notes: We plot the Ca content of osteon and CL versus the Ca content of osteon. First, we see a correlation between the Ca content of CL and of osteon. Then, looking at the difference between the two lines, we clearly see that at low mineralized osteon, we have a high difference in terms in mineral content between the CL and the osteon. Difference which decreases with osteon mineralization. This suggests that we have different mineralization kinetics for CL and osteons, which is in agreement with a previous study from Milovanovic.
Now, looking more locally and based on our previous observations, we represent the correlation between the Ca content of the outside and of the CL for different level of osteon mineralization. For young osteon, this correlation is strong, the outside envrionment is clearly influencing the composition of the CL. Then, this correlation decreases with time but increases again for the oldest osteons, probably due to a state of saturation for both older bone and CL.

## Slide 19: CL stiffer in contradiction with previous studies
[1] Bobji et al., JMR, 1998
Zhou et al., EMI, 2020:
Hydrated samples
Higher roughness (in view of the surface profile)
Peak force tapping AFM with setpoint force of 400 nm
No imaging technique to highlight the CL beforehand, no information about how they distinguish CL from surrounding bone
Our research
Dehydrated samples
Low roughness ~ 10 nm
Standard nanoindentation with force of 500 µN and penetration of ~ 150 nm
qBEI used to highlight the CL pre-nIND + location of indents wrt CL post-nIND
Hydration has an impact on mechanical properties, but dehydration and embedding enable to reach a better roughness
Influence of roughness on measurements when indentation depths are not much greater than surface roughness (threshold of 10 x higher recommended) [1]
 There is no way of confirming CL location without using another imaging technique
Notes: Today this is the best way to obtain a really accurate and local anlaysis of the mechanical properties as required by the thickkness of cement lines (we need a perfect surface)

## Slide 20: CL stiffer in contradiction with previous studies
Montalbano et al., J. Mater. Res., 2011:
Lateral spacing of 2.25 µm
Optical images to highlight CL location
Softer regions measured ~ 4.5 µm which is the upper limit of CL:
  Surface anomaly
  Indentation convolution (CL + surrounding bone)
  Coexistence of CL & soft lamella
Our research
Lateral spacing of 1 µm
qBEI used to highlight the CL pre-nIND + location of indents wrt CL post-nIND
Usually not striking, probably nanoindentation convolution too (stiffer part = CL + interstitial bone or older osteon)
Thickness of CL: 1-3 µm
Do we really see CL in optics? From the figure we cannot tell…

## Slide 21: qBEI Calibration
When sending a beam of electrons over a sample, electrons interact with atoms, producing various signals (including BE)
BE are electrons from the beam that are reflected back because they are deviated by atom nuclei
Therefore, BE signal is highly sensitive to the local atomic number (Z): the higher the atomic number of the atoms hit by the beam, the higher the BE signal
Bone is a heterogeneous material, composed of varying proportion of:
  Organic matrix: Z ~ 6
  Hydroxylapatite Ca5(PO4)3OH: Z ~ 14.06
The constituent with the highest atomic number dominantly influences the BEs intensity (Ca, Z = 20)

## Slide 22: qBEI Calibration
Adjust machine parameters to get GL of 2 reference materials:
- GL(C) = 25
- GL(Al) = 225
Define calibration line with those points
Measure experimentally osteoid GL and fix it as 0 wt% Ca standard
Pure HA is 39.86 wt% Ca, and measure its GL from calibration line (known Zmean = 14.06)
Define standardization line from those points
How can we connect grey level (GL) to local Ca concentration ?

## Slide 23: SHG
Harmonic Generation: Optical effect in which k photons with the same frequency interact with a material and generate a new photon with k times the energy (& the frequency) of the initial photons
Second-Harmonic Generation (SHG): special case in which there are two photons (k = 2)  frequency doubling
Only specific types of medium are able to produce SHG signal. The most important prerequisite condition being that at the molecular level, the material must have no center of symmetry  several biological tissues meet these requirements, including collagen type I and III, and myosin.
Strong SHG signal is usually generated by regions with densely packed collagen fibrils, preferentially arranged parallel to the imaging plane
If collagen fibrils are oriented out of the image plane, no signal should be detected
Notes: Using a laser able to generate intense light and specific filters, the emitted signal can be easily extracted as its frequency is twice the one of the excitation.
To produce an efficient signal, molecules should be aligned within the image plane, as illustrated in Figure
The intensity of the signal also depends on the collagen concentration, the degree of order, the diameter of the fibrils [82] and the amount of cross linking of collagen. SHG imaging is a powerful technique as it provides endogenous contrast for collagen without the need for staining, its main limitation being related to the proper quantification of the signal,
which, given the confounded parameters of influence just mentioned, remains delicate.

## Slide 24: Nanoindentation
Based on Oliver Pharr model which assumes that elastic and plastic deformations during loading and only elastic displacements recovered during unloading
Berkovitch tip  β
From P-h curves: max load, max displacement and elastic unloading stiffness
From calibration in FQ (reference material): contact area 
Hardness estimation:
Elastic modulus measurements (derived from eastic contact theory):
Er accounts for elastic displacement in both sample and tip

## Slide 25: Methods
nIND:
  Berkovitch tip (50 nm tip radius)
  Displacement controlled trapezoidal load function
  Max load of 500 µN with penetration depth of ~150 nm
  Average roughness of ~10 nm
  Lateral spacing of 1 µm

## Slide 26: SRµCT
Synchrotron radiation is a specific radiation emitted by charged particles when they are subject to an acceleration perpendicular to their velocity  It happens for example when electrons are moving fast through magnetic fields, which is the case in a synchrotron facility.
X-ray scattering: Quantitative information on the arrangement of atoms in crystals molecules and supramolecular entities in biomaterials at 0.1-100 nm
  Small angle X-ray scattering SAXS: Orientation (rho-parameter), size & shape (T-parameter) of mineral platelets
  Wide angle X-ray scattering WAXS: Orientation of crystalline c-axis and mean length of mineral platelets (L-parameter)

## Slide 27: CLS
High-resolution optical imaging technique with depth selectivity to do optical sectioning (3D reconstruction) and to obtain fluorescence-based images
Principle:
Laser light emitted from collimated laser beam
Light reflected by dichroic mirror
Light passing through the objective lens which focuses it onto a defined spot at a specific depth within the sample
Emission of fluorescent light at this point
Out-of focus light cut off by a pinhole so that only fluorescence signals from the illuminated spot enter the detector
Ghafoor, PhD thesis, 2017

## Slide 28: CLS processing
Skeletonization: Transformation process that reduces a volumetric object into a significantly reduced, simplified and compact representation, while preserving the topology (connectivity, edge length, orientation) and geometric properties of the object.
Method for the osteocyte lacuno-canalicular network:
Extraction of the location of the canaliculi and junctions (nodes) between them
Thinning algorithm applied to the binarized and segmented image data to obtain the center line or medial axis of the canaliculi → Voxels iteratively removed from the surface volume if removing them did not change the connectivity of the 3D neighborhood and if they were not endpoints
Skeleton converted into mathematical network consisting of nodes and edges using specialized software (e.g. Skan, Python library)
Van Tol et al., Biomech Model Mechanobiol, 2020

## Slide 29: Correlation of CL mineral content with inside & outside
R² = 0.36
p <0.05
R² = 0.21
p <0.05
R² = 0.41
p <0.05
R² = 0.78
p <0.05
R² = 0.15
p <0.05
R² = 0.07
p <0.05
R² = 0.01
p = 0.23
R² = 0.18
p <0.05
R² = 0.09
p <0.05
R² = 0.05
p <0.05
R² = 0.25
p < 0.05
R² = 0.64
p <0.05
R² = 0.03
p = 0.05
R² = 0.04
p <0.05
R² = 0.04
p <0.05
R² = 0.25
p <0.05

## Slide 30: Correlation of CL mineral content with equal bins
R² = 0.35
p <0.05
R² = 0.18
p <0.05
R² = 0.47
p <0.05
R² = 0.77
p < 0.05
R² = 0.15
p <0.05
R² = 0.02
p = 0.07
R² = 0.22
p <0.05
R² = 0.11
p <0.05
R² = 0.36
p <0.05
R² = 0.21
p <0.05
R² = 0.41
p <0.05
R² = 0.78
p <0.05
R² = 0.15
p <0.05
R² = 0.07
p <0.05
R² = 0.01
p = 0.23
R² = 0.18
p <0.05
21-24 wt %
6 osteons
24-25 wt %
9 osteons
25-25.5 wt %
13 osteons
25.5-26.5 wt %
7 osteons
21-24.61
wt %
9 osteons
24.62-25.13
wt %
9 osteons
25.14-25.47
wt %
9 osteons
25.48-26.5
wt %
8 osteons
Ca content
Number of osteons