## Slide 1
PARAMETRIC EXPERIMENTAL STUDY ON GLT COLUMNS STABILITY
DURING NATURAL FIRE TESTS INCLUDING THE COOLING PHASE
Silvio RENARD, Fabienne ROBERT Fire Testing Centre, CERIB France
Thomas GERNAY Johns Hopkins University USA
Jochen ZEHFUSS Techn. Univ. Braunschweig Germany
Robert MCNAMEE RISE Res. Inst. of Sweden and Lund Univ. Sweden
Patrick BAMONTE Politecnico di Milano Italy
Jean-Marc FRANSSEN Univ. of Liege Belgium

## Slide 2
1. The context
1.1 Unprotected Glue Laminates Timber columns
in short, unattended non-standard fires
1. The context
Fire Resistance Rating
time
T

## Slide 3
1) The heat wave continues propagating in the section after the peak of the fire.
2) Temperatures in the centre of a timber section as low as 200°C or 100°C
lead to a significant reduction of compressive strength.
1. The context
1.1 Timber columns in non-standard fires
1.2 General concern

## Slide 4
Gernay, Fire resistance and burnout resistance of timber columns, Fire Safety Journal, 122, 103350, 2021
1. The context
1.1 Timber columns in non-standard fires
1.2 General concern
1.3 Numerical analyses with SAFIR®
Fire Resistance Rating
t
T
Fire Resistance Rating
t
T
Green zone = 0,2 to 0,5 FRR
DHP
DHP

## Slide 5
1. The context
1.1 Timber columns in non-standard fires
1.2 General concern
1.3 Numerical analyses with SAFIR®
1.4 Furnace tests (iBMB, Braunschweig)

## Slide 6
Loaded unprotected GLT Column, 28 cm x 28 cm, designed to have a FRR of 60 minutes.
Gernay et al., Experimental investigation of structural failure during the cooling phase of a fire: Timber columns, Fire and Materials, 1-16, 2022
Rmean = 56,5 min.
(55 and 58 min.)

## Slide 7
Same columns, heating for 10 minutes (0,18 x Rmean) => cooling at -10°C/min
-10°C/min
10
No collapse
(2 specimens)

## Slide 8
Same columns, heating for 15 minutes (0,27 x Rmean) => cooling at -10°C/min
-10°C/min
15
Collapse after 98 and 153 minutes (2 specimens)

## Slide 9
1. The context
1.1 Timber columns in non-standard fires
1.2 General concern
1.3 Numerical analyses with SAFIR®
1.4 Furnace tests (iBMB, Braunschweig)
1.5 Compartment fires (CERIB, France), series 1.
Robert et al., Natural fire tests on GLT columns including the cooling down phase, WCTE, Oslo 2023, 1848-1854

## Slide 10
The compartment
Length: 6 meters
Width: 4 meters
Height: 3,10 meters

## Slide 11
950 MJ/m²
≈ 80% fractile for dwellings in EC1
1 test
420 MJ/m²
Average value for offices in EC1
1 test
780 MJ/m²
≈ average value for dwellings in EC1
5 tests
The fire loads

## Slide 12
The openings
O = 0.032 m^0.5: 1 test
O = 0,065 m^0.5: 5 tests
O = 0.144 m^0.5: 1 test

## Slide 13
The column
L = 3,72 meters - Pinned-pinned;
N = 322 kN - e = 20 mm / 20 mm
Section;
28 x 28 cm² : 5 tests (same as in Braunschweig)
34 x 34 cm² : 1 test
36 x 36 cm² : 1 test

## Slide 14
34 x 34
36 x 36
Instability of the loading system 

## Slide 15
1. The context
1.1 Timber columns in non-standard fires
1.2 General concern
1.3 Numerical analyses with SAFIR®
1.4 Furnace tests (iBMB, Braunschweig)
1.5 Compartment fires (CERIB, France), series 1.
1.6 Conclusions of series 1.3, 1.4 and 1.5
Timber columns can collapse in the decay or the cooling phase of a fire.
Self-extinction of the column does not solve the problem.

## Slide 16
The context
New compartment fires (CERIB, series 2.)
1) Lower temperatures in the compartment: Test 17 (thicker sticks)
28 x 28 cm²

## Slide 17
The context
New compartment fires (CERIB, series 2.)
28 x 28 cm²
1) Lower temperatures in the compartment: Test 17 (thicker sticks)

## Slide 18
New compartment fires (CERIB, series 2.)
Lower temperatures in the compartment: Test 17
Increased section size 40 x 40 cm²: Tests 18, 19, 20

## Slide 19
Test 18
Survival  ….
until 11 hours 28 minutes 

## Slide 20
Test 18
Yet, local defect in the gluing plane, filled with intumescent paint.

## Slide 21
Test 18
Conclusions of Test 18:
Cannot be considered to derive a calculation method.
Influence of longitudinal cracks…
if the member is left unattended after the fire

## Slide 22
Test 19 = Test 18 without any thermocouple inside
Survival  ….
until 16 hours 18 minutes 

## Slide 23
Test 19
Yet, local glowing / smouldering at the foot of the column.
Foot of the columns after the test
Residual section
after the test
at mid-level
at the foot

## Slide 24
Test 19
Yet, local glowing / smouldering at the foot of the column.
Foot of the columns after the test
Explanation
???
Also observed by
Wiesner et al., Fire Techn., 2021
Mitchell et al., FSJ, 2023

## Slide 25
Test 20, reduced temperatures (thicker sticks)
Survival  ….
until 12 hours 18 minutes 

## Slide 26
Test 20, reduced temperatures
Survival  ….
until 12 hours 18 minutes 
Again with smouldering at the foot

## Slide 27
New compartment fires (CERIB, series 2.)
Lower temperatures in the compartment: Test 17
Increased section size 40 x 40 cm²: Tests 18, 19 20
Fire fighters' intervention: Test 21 (28 x 28 cm², thick sticks)
At 35 minutes, fire fighters:
extinguished the wood cribs from outside,
sprayed the column,
Scratched the charred layers away.
Survival 

## Slide 28
Nothwistanding this aggressive intervention (2, fire men; 1 m3 of water + scratching)
temperatures in the centre of the column increased until 4 hours !

## Slide 29: Test 21 – TCs measurement

## Slide 30
Conclusions at this stage:
Collapse can occur in the decay or cooling phase of a fire.
Severe influence of longitudinal cracks.
Smouldering at the foot, still to be explained.
Never leave a timber column unattended after a fire,
collapse can occur after several hours.
Rapid extinction is a must.

## Slide 31
Thank you
Test data on : https://www.burnout-resistance.eu/