## Slide 1
Abdul Herrim SEIDOU
Materials Engineer / PhD Candidate
Metallic Materials Science Unit (MMS)
University of Liège, Belgium
ahb.seidou@uliege.be
Evaluation of Corrosion Resistance of 316L stainless steel with or without SiC additions produced via Directed Energy Deposition
Corrosion tests performed in 0.5M NaCl (aq) solution at room temperature
Direct Energy Deposition (DED)
For system stabilization
Bode and Nyquist plots for general corrosion evaluation
PDP curve for pitting corrosion
Open Circuit
Polarization (OCP) ~ 15h
Electrochemical Impedance Spectroscopy (EIS)
Potentiodynamic Polarization (PDP)
Materials tested
316L stainless steel (wrought)
316L stainless steel DED
316L + 10 vol.% SiC DED
316L + 20 vol.% SiC DED
High build rates
Can be used for repair
Multi-material range
Reduced material waste
Advantages of DED:

## Slide 2
Abdul Herrim SEIDOU
Materials Engineer / PhD Candidate
Metallic Materials Science Unit (MMS)
University of Liège, Belgium
ahb.seidou@uliege.be
EIS for general corrosion
Potentiodynamic polarization for passivation and pitting corrosion
SEM micrographs after potentiodynamic polarization