## Slide 1
Microstructural and Defects investigation of AlCrFeMnNi-based High Entropy Alloy fabricated via Laser Powder Bed Fusion
SEIDOU A. Herrim, BLONDIAU Catherine, DEDRY Olivier, TCHUINDJANG Jérôme Tchoufang and MERTENS Anne
Metallic Materials Science (MMS), Aerospace and Mechanical Engineering Dpt., University of Liège, Belgium
07/05/2025

## Slide 2
HEAs
CCAs
5+ elements
Single-phase solid solution
High configurational entropy
May have <5 elements
>35% of elements
Multiple phases, Intermetallics (IM) included
Introduction
FCC-based HEAs
Better corrosion resistance
Better ductility
BCC-based HEAs
High strength
Good electrical and thermal conductivity
Low thermal expansion
The common phases are FCC and BCC, while the IM are B2, Sigma and Laves.
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
The goal of this study is to design a corrosion-resistant HEA through LPBF
[Odetola et al. (2024)]
Notes: This work aim to investigate the effects of the selected elements into the microstructure, and to understand the near-equilibrium mechanisms and phenomena.

## Slide 3
CrFeMnNi-based MEA and AlCrFeMnNi-based HEA: Solidification sequence
Differential Thermal Analysis
In AlCrFeMnNi system, FCC phase is Cr-Fe rich while BCC phase is rich in Al and Ni
Al promotes the BCC formation, followed by spinodal decomposition
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
[Seidou et al. (2024)] Esaform2024

## Slide 4
Fe | C | Cr | Ni | Mo | Mn | Si
Bal. | 0.03 | 18 | 14 | 3 | 2 | 1
AISI 316L SS
Materials and Methods
Aconity MINI
Laser Powder Bed Fusion machine
Al0.2Cr0.7Fe1.8MnMo0.1Ni1.5 was printed, targeting an FCC microstructure
The powder mixture was prepared using AISI 316L SS and elemental powders
Powders obtained by Gas Atomization
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
With manual mixing
[https://www.mmsonline.com/kc/additive_manufacturing_for_production/metal-parts]
LPBF process
4

## Slide 5
Parameters:
Scanning speed (mm/s): 200 to 2000
Laser power (W): 50 to 200
  -> Energy (J/mm): 0,042 to 1
Al0.2Cr0.7Fe1.8MnMo0.1Ni1.5
Single tracks for parameters optimization
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
5
53 sets of parameters were investigated to narrow the range of optimal parameters.
[Yadroitsev, I., & Smurov, I. (2010). Selective laser melting technology: From the single laser melted track stability to 3D parts of complex shape. Physics Procedia, 5, 551-560]
Results and discussion

## Slide 6
Parameters:
Scan strategy: Bidirectional 90°
Remelting for better homogeneity
Pre-heating at 200°C
  To avoid cracks and delamination
[J/mm3]
Volumetric Energy Density
Al0.2Cr0.7Fe1.8MnMo0.1Ni1.5
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
6
Increasing Ed
Printing parameters selected from single tracks optimization

## Slide 7
1
2
3
4
5
6
7
8
9
10
15
14
13
12
11
16
17
18
19
20
1
2
3
4
5
6
7
8
9
10
15
14
13
12
11
16
17
18
19
20
X
X
Highest Ed
20 cubes 10 x 10 x 10 mm
Al0.2Cr0.7Fe1.8MnMo0.1Ni1.5
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
[J/mm3]
Volumetric Energy Density
Printing parameters selected from single tracks optimization
7
Increasing Ed
.
BD

## Slide 8
Hots cracks and elemental agglomerates in all the samples, including the ones with remelting.
Fluctuations within the meltpools, Mo agglomerates, and hot cracks are observed.
Sample 3: P=150W, vs=800mm/s
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
Etched with Nital
As polished
8
SEM micrographs revealing microstructural defects
Sample 17: P=175W, vs=800mm/s, remelting

## Slide 9
Sample 17: P=175W, vs=800mm/s, remelting
Sample 3: P=150W, vs=800mm/s
The dissolution of refractory element (Mo) is limited, causing microstructural heterogeneity.
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
9
SEM micrographs revealing microstructural defects

## Slide 10
EDS elemental map showing compositional heterogeneity in the meltpool
Sample 3: P=150W, vs=800mm/s
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
10

## Slide 11
Sample 17: P=175W, vs=800mm/s, remelting
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
11
EDS elemental map showing compositional heterogeneity in the meltpool

## Slide 12
Sample 17: P=175W, vs=800mm/s, remelting
Sample 3: P=150W, vs=800mm/s
Initiation of hot cracks during solidification in LPBF
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
12
[Guo et al., Effects of elemental segregation and scanning strategy on the mechanical properties and hot cracking of a selective laser melted FeCoCrNiMn-(N, Si) high entropy alloy, J. Alloys Compd., 865 (2021) 158892]
Hot cracks can develop in the last liquid rich in Si that solidifies at high angle grain boundaries.

## Slide 13
Using elemental and alloy powder mixtures in LPBF allows testing multiple compositions without costly atomization.
Key challenges include partial or non-dissolution of refractory elements (Mo) and powder size effects, leading to agglomerates or comet tails in the melt pool.
Rapid cooling in LPBF causes compositional heterogeneity and elemental segregation (Si), increasing the risk of hot cracks.
Addressing these issues is crucial for HEA development: refining refractory powder size improves dissolution, while commercial pre-alloyed powders reduce reliance on elemental powders.
Conclusions
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
13

## Slide 14
Perspectives
Use spherical commodity powders such as 316L SS, NiCr 80:20 to reach a specific composition.
Investigate the as-built microstructure.
Use custom made pre-alloyed powders if defects such as hot cracks cannot be avoided.
Perform corrosion tests such as Electrochemical Impedance Spectrometry (EIS), Potentiodynamic polarization (PDP), Cyclic potentiodynamic polarization (CPDP).
International Esaform Conference 2025
07-09 May 2025 / Paestum, Italy
14

## Slide 15
Thanks for your attention
Herrim Seidou, PhD candidate
Ahb.seidou@uliege.be
Metallic Materials Science (MMS) team
Aerospace and Mechanical Engineering Dpt.
University of Liège, Belgium
All publications of the Metallic Materials Science team are available at : https://orbi.uliege.be/

## Slide 16
Sample 17: P=175W, vs=800mm/s, remelting
Sample 3: P=150W, vs=800mm/s
Average grain size = 32µm
Average grain size = 40.2 µm
Misorientation angle
Misorientation angle
HAGB
LAGB

## Slide 17
Sample 3: P=150W, vs=800mm/s
Misorientation Profiles

## Slide 18
Sample 17: P=175W, vs=800mm/s, remelting
Misorientation Profiles