## Slide 1
📅 11/09/2024
✉ laura.muller@uliege.be
🌐 www.biomat.uliege.be
Microstructural and micromechanical analysis of proximal tibia in aging rats
Laura Müller 1, Margaux Ska 1, Piyush Uniyal 2, G. Harry van Lenthe 2 and Davide Ruffoni 1
1 University of Liège, Belgium
² KU Leuven, Belgium

## Slide 2: The Impact of Aging on the Proximal Tibia
How do age-related microstructural alterations impact the strain distribution in the epiphysis of the proximal rat tibia?
Epiphysis
Metaphysis
Growth Plate
Tibia
Femur
1/10
Notes: The proximal tibia is a region of high biomechanical importance that helps to distribute forces and prevent stress concentrations.

## Slide 3: Methods
Animal model: Wistar Rats
Adult 3 months (n=6)
Old 13 months (n=6)
Microstructure
µCT - 10 µm
Material properties
Elastic modulus
Nanoindentation
1.5 µm
3 mm
Mechanical properties
2/10
Strain distribution
Simulation
10 µm

## Slide 4: Microstructural changes with age
Old
Adult
Trabecular bone
BV/TV decreases & Network becomes coarser
Same behaviour in the Metaphysis
Young
Old
50
0
100
150
Tb.Th [µm]
Young
Old
100
0
200
300
400
Cort.Th [µm]
Young
Old
100
0
200
300
400
Th.Sp [µm]
Young
Old
10
0
20
30
50
BV/TV [%]
40
Young
Old
4
0
8
10
BB/TV [%]
6
2
-12%*
+23%*
+51%*
+86%*
Young
Old
100
0
300
400
GP.Th [µm]
200
-53%*
+18%*
3/10

## Slide 5: Microstructural changes with age
Old
Adult
Cortical bone
Subchondral bone plate thickness increases
3/10
Young
Old
50
0
100
150
Tb.Th [µm]
Young
Old
100
0
200
300
400
Cort.Th [µm]
Young
Old
100
0
200
300
400
Th.Sp [µm]
Young
Old
10
0
20
30
50
BV/TV [%]
40
Young
Old
4
0
8
10
BB/TV [%]
6
2
-12%*
+23%*
+51%*
+86%*
Young
Old
100
0
300
400
GP.Th [µm]
200
-53%*
+18%*

## Slide 6: Microstructural changes with age
Old
Adult
Growth Plate
Thickness increases
Number of bone bridges increases
3/10
Young
Old
50
0
100
150
Tb.Th [µm]
Young
Old
100
0
200
300
400
Cort.Th [µm]
Young
Old
100
0
200
300
400
Th.Sp [µm]
Young
Old
10
0
20
30
50
BV/TV [%]
40
Young
Old
4
0
8
10
BB/TV [%]
6
2
-12%*
+23%*
+51%*
+86%*
Young
Old
100
0
300
400
GP.Th [µm]
200
-53%*
+18%*

## Slide 7: Methods: Mechanical properties
Simulation
Parosol software
Linear elastic solution
NIC5 cluster (ULiege)
Loaded surface
F = 40N
Bone Materials
Homogeneous, elastic, isotropic
Poisson ratio 0.3
Young’s modulus 25 GPa
Mesh
µCT-based FE models
Hexahedral elements
10 µm length
Top view
Constrained plane
4/10
n = 6/group
Outcomes
Effective strain

## Slide 8
Anterior
Posterior
Anterior
Posterior
Adult tibia
Old tibia
5e-04
4
3
2
1
0
Effective strain [-]
5e-04
4
3
2
1
0
Effective strain [-]
5/10
Influence of microstructure on mechanical properties

## Slide 9: Methods: Mechanical properties
Simulation
Parosol software
Linear elastic solution
NIC5 cluster (ULiege)
Loaded surface
F = 40N
Bone Materials
Homogeneous, elastic, isotropic
Poisson ratio 0.3
Young’s modulus 25 GPa
Mesh
µCT-based FE models
Hexahedral elements
10 µm length
Constrained plane
6/10
n = 2 young and 1 old samples
Outcomes
Effective strain
Growth Plate
Sagittal section
Growth Plate Materials
Homogeneous, elastic, isotropic
Poisson ratio 0.3
Young’s modulus 5 MPa, 50 MPa and 500 MPa

## Slide 10
Anterior
Posterior
Anterior
Posterior
0 MPa
5 MPa
50 MPa
500 MPa
0 MPa
5 MPa
50 MPa
500 MPa
7/10
5e-04
4
3
2
1
0
Effective strain [-]
5e-04
4
3
2
1
0
Effective strain [-]
Adult tibia
Old tibia
Mechanical properties: Addition of a growth plate

## Slide 11
6e-04
8/10
Adult tibia
Cortical
Trabecular
Cortical
Trabecular
2
0
3
Mean effective strain [-]
5
4
1
With more bone bridges
With few bone bridges
Old tibia
6e-04
2
0
3
Mean effective strain [-]
5
4
1
Without growth plate
Growth plate of 5 MPa
Growth plate of 50 MPa
Growth plate of 500 MPa
Without growth plate
Growth plate of 5 MPa
Growth plate of 50 MPa
Growth plate of 500 MPa
Cortical
Trabecular
Mechanical properties: Addition of a growth plate

## Slide 12
6e-04
9/10
Old tibia
Cortical
Trabecular
Cortical
Trabecular
Cortical
Trabecular
2
0
3
Mean effective strain [-]
5
4
1
6e-04
2
0
3
Mean effective strain [-]
5
4
1
Adult tibia
Growth plate of 50 MPa
Growth plate of 50 MPa
With more bone bridges
With few bone bridges
Influence of microstructure on mechanical properties

## Slide 13
6e-04
9/10
Old tibia
Cortical
Trabecular
Cortical
Trabecular
Cortical
Trabecular
2
0
3
Mean effective strain [-]
5
4
1
With bone bridges
6e-04
2
0
3
Mean effective strain [-]
5
4
1
Adult tibia
Growth plate of 50 MPa
Growth plate of 50 MPa
2e-04
Cortical
Trabecular
0
1
Mean effective strain [-]
1.5
0.5
Old samples
Adult samples
50 MPa
With few bone bridges
Influence of microstructure on mechanical properties

## Slide 14
10/10
Conclusion
Importance of the growth plate in the simulations
Findings
Increasing the number of samples to study
Future works
RESULTS
Young's modulus of at least 50 MPa for the growth plate
Refining the Young's modulus value of the growth plate
Changing the load direction

## Slide 15
Pierre
DRION
University of Liège, Belgium
Davide
RUFFONI
Piyush Uniyal
Harry
van Lenthe
Katholieke Universiteit Leuven, Belgium
University of Liège, Belgium
10/10
Thanks to all co-authors!
Margaux
SKA

## Slide 16
Thank you for your attention!
Any questions?
Laura Müller
@Mllr_Laura

## Slide 17
2e-04
9/10
Cortical
Trabecular
0
1
Mean effective strain [-]
1.5
0.5
Mechanical properties: The effect of aging
Old samples
Adult samples
50 MPa
2e-04
Cortical
Trabecular
0
1
Mean effective strain [-]
1.5
0.5
Old samples
Adult samples
500 MPa

## Slide 18
Nanoindentation
  Berkovitch tip (50 nm tip radius)
  Displacement controlled trapezoidal load function
  10s loading, 15s holding, 10s unloading
  Penetration depth of ~150 nm
  Lateral spacing of 1.5 µm

## Slide 19: Nanoindentation
Based on Oliver Pharr model which assumes that elastic and plastic deformations during loading and only elastic displacements recovered during unloading
Berkovitch tip  β
From P-h curves: max load, max displacement and elastic unloading stiffness
From calibration in FQ (reference material): contact area 
Hardness estimation:
Elastic modulus measurements (derived from eastic contact theory):
Er accounts for elastic displacement in both sample and tip

## Slide 20: ParoSol simulations
MATERIAL ASSIGNMENT
Poisson’s ratio 0.3
Young’s modulus
  ADULT 25.53 GPa
  OLD 29.56 GPa
BONE
GROWTH PLATE
Poisson’s ratio 0.3
Young’s modulus
  PHYSIOLOGICAL 5 and 50 MPa
  PATHOLOGICAL 500 MPa
MESH ASSIGNMENT
10 µm length

## Slide 21
6e-04
8/10
Adult tibia
Cortical
Trabecular
2
0
3
Mean effective strain [-]
5
4
1
Old tibia
6e-04
2
0
3
Mean effective strain [-]
5
4
1
Without growth plate
Growth plate of 5 MPa
Growth plate of 50 MPa
Growth plate of 500 MPa
Without growth plate
Growth plate of 5 MPa
Growth plate of 50 MPa
Growth plate of 500 MPa
Cortical
Trabecular
Mechanical properties: Addition of a growth plate