## Slide 1
📅 03/07/2024
✉ laura.muller@uliege.be
🌐 www.biomat.uliege.be
Changes in Mineral Content and Mechanical Properties of Calcified Cartilage in the Knee during Aging
Laura Müller 1, Stéphane Blouin2, Pierre Drion 1, Markus A. Hartmann2, Davide Ruffoni 1
1 University of Liege, Liege, Belgium ; ² Ludwig Boltzmann Institute of Osteology, Vienna, Austria
Musculoskeletal biomechanics VII: Soft tissues and interfaces

## Slide 2: The Impact of Aging on the Proximal Tibia
1/10
Osteochondral junction
Femur
Tibia
Uncalcified cartilage (UC)
Subchondral bone (SB)
Calcified cartilage (CC)
Clinical relevance:
Aging is the main risk factor of joint diseases
Materials engineering:
Attachment of dissimilar materials on a very small area
20 MPa
20 GPa
~80 µm

## Slide 3: A Multimodal Analysis of Proximal Tibia
2/10
Animal model: Wistar Rats
Adult 3 months (n=6)
Old 13 months (n=6)
Microstructure
µCT – 10 µm
Loss of trabecular BV/TV
Increase of thickness subchondral plate
Mineral content
Mechanical properties
Quantitative backscattered electron microscopy
qBEI – 0.88 µm
Nanoindentation Lateral spacing : 1.5 µm
3 mm
Ca [wt%]
250 µm
30 µm
CC
SB
CC
E [GPa]
H [GPa]
Ludwig Boltzmann Institute of Osteology

## Slide 4: Qualitative Analysis of Mineral Content
4/10
Uncalcified Cartilage
Calcified Cartilage
Subchondral Bone
Aging:
Thickening of calcified cartilage
Mineralization of chondrocytes lacunae
Reduced roughness at the tidemark due to less chondrocytes
Old
Adult
Cement Line
100 µm
100 µm

## Slide 5: Qualitative Analysis of Mineral Content
4/10
Uncalcified Cartilage
Calcified Cartilage
Subchondral Bone
Aging:
Thickening of calcified cartilage
Mineralization of chondrocytes lacunae
Reduced roughness at the tidemark due to less chondrocytes
Old
Adult
Cement Line
100 µm
100 µm
Mineralized lacunae

## Slide 6: Qualitative Analysis of Mineral Content
4/10
Uncalcified Cartilage
Calcified Cartilage
Subchondral Bone
Aging:
Thickening of calcified cartilage
Mineralization of chondrocytes lacunae
Reduced roughness at the tidemark due to less chondrocytes
Old
Adult
Cement Line
100 µm
100 µm
Mineralized lacunae

## Slide 7: Qualitative Analysis of Mineral Content
4/10
Uncalcified Cartilage
Calcified Cartilage
Subchondral Bone
Aging:
Thickening of calcified cartilage
Mineralization of chondrocytes lacunae
Reduced roughness at the tidemark due to less chondrocytes
Old
Adult
Cement Line
100 µm
100 µm
Mineralized lacunae

## Slide 8: Frequency Distribution of Mineral Content
20
15
25
30
35
Ca [wt%]
0
0.1
0.2
Frequency [%]
0.25
0.15
0.05
5/10
Adult Bone
Adult Cartilage

## Slide 9: Frequency Distribution of Mineral Content
20
15
25
30
35
Ca [wt%]
0
0.1
0.2
Frequency [%]
0.25
0.15
0.05
5/10
Adult Bone
Old Bone
Adult Cartilage
Old Cartilage

## Slide 10: Frequency Distribution of Mineral Content
20
15
25
30
35
Ca [wt%]
0
0.1
0.2
Frequency [%]
0.25
0.15
0.05
5/10
-7%*
Ca Mean [wt%]
Ca Width [wt%]
6
4
2
0
-2%
Adult
Old
Adult
Old
+6%*
+10%*
30
20
10
0
Adult
Old
Adult
Old
Bone
Cartilage
Adult Cartilage
Old Cartilage
Adult Bone
Old Bone
*p-value: 0.05

## Slide 11: Frequency Distribution of Mineral Content
20
15
25
30
35
Ca [wt%]
0
0.1
0.2
Frequency [%]
0.25
0.15
0.05
5/10
-7%*
Ca Mean [wt%]
Ca Width [wt%]
6
4
2
0
-2%
Adult
Old
Adult
Old
+6%*
+10%*
30
20
10
0
Adult
Old
Adult
Old
Bone
Cartilage
Adult Cartilage
Old Cartilage
Adult Bone
Old Bone
*p-value: 0.05

## Slide 12: Frequency Distribution of Mineral Content
20
15
25
30
35
Ca [wt%]
0
0.1
0.2
Frequency [%]
0.25
0.15
0.05
5/10
-7%*
Ca Mean [wt%]
Ca Width [wt%]
6
4
2
0
-2%
Adult
Old
Adult
Old
+6%*
+10%*
30
20
10
0
Adult
Old
Adult
Old
Bone
Cartilage
Adult Cartilage
Old Cartilage
Adult Bone
Old Bone
*p-value: 0.05

## Slide 13: Mineral Gradients across Cartilage Interface
30
20
10
0
Ca Content [wt%]
0
-5
5
10
15
Distance [µm]
30
20
10
0
Ca Content [wt%]
0
-5
5
10
15
6/10
Distance [µm]
Calcified
Uncalcified
UC
CC
SB
UC
CC
SB
Calcified
Uncalcified
Old
Adult
Average
Sigmoid fit
Average
Sigmoid fit
15 µm
22 µm

## Slide 14: Indentation Modulus Maps in Mineralized Cartilage
7/10
Indentation
Modulus [GPa]
30
0
15
Ca Content [wt%]
45
0
15
30
Indentation
Modulus [GPa]
30
0
15
Ca Content [wt%]
45
0
15
30
Old
Adult
50 µm
30 µm
30 µm
UC
CC
UC
CC
UC
CC
CC
UC

## Slide 15: Quantitative Analysis in Mineralized Cartilage
8/10
H [GPa]
1
0.7
0.3
0
Adult
Old
+2%
E [GPa]
30
20
10
0
+28%*
Adult
Old
*p-value: 0.05
Stiffness
Hardness

## Slide 16: Quantitative Analysis in Mineralized Cartilage
8/10
H [GPa]
1
0.7
0.3
0
Adult
Old
+2%
E [GPa]
30
20
10
0
+28%*
Adult
Old
0.06
0.04
0.02
0
H/E [-]
Adult
Old
-14%*
*p-value: 0.05
Stiffness
Hardness
Ratio Hardness/Stiffness

## Slide 17: Conclusion
9/10
Analyses show significative changes in the proximal tibia's microstructure, mineral content, and stiffness with age
Strains & Displacements distribution
µCT & Digital volume correlation
Supported by mobility grant ESB
Enrico Dall’Ara
Sriram Kunnoth

## Slide 18
University of Liege, Belgium
Davide
RUFFONI
Pierre
DRION
Stéphane BLOUIN
Markus
HARTMANN
Ludwig Boltzmann Institute of Osteology, Austria
University of Liège, Belgium
10/10
Thanks to all co-authors!

## Slide 19
Thank you for your attention!
Any questions?
Laura Müller
@Mllr_Laura

## Slide 20: Quantitative Analysis in Mineralized Cartilage
H [Gpa]
1
0.7
0.3
0
Adult
Old
+2%
E [Gpa]
30
20
10
0
+28%*
0.06
0.05
0.04
0.03
0.02
0.01
0
Adult
Old
H/E [-]
In homogenoeus material, H = Constant*
= E

## Slide 21: Quantitative Analysis in Mineralized Cartilage
H [Gpa]
1
0.7
0.3
0
Adult
Old
H [GPa]
1
0.7
0.3
0
H [GPa]
1
0.7
0.3
0
20
0
5
10
-5
Distance [µm]
20
0
5
10
-5
Distance [µm]
+2%
E [Gpa]
30
20
10
0
+28%*
E [GPa]
30
20
10
0
20
0
5
10
-5
Distance [µm]
E [GPa]
30
20
10
0
20
0
5
10
-5
Distance [µm]
Adult
Old

## Slide 22
Nanoindentation
  Berkovitch tip (50 nm tip radius)
  Displacement controlled trapezoidal load function
  10s loading, 15s holding, 10s unloading
  Penetration depth of ~150 nm
  Lateral spacing of 1.5 µm

## Slide 23: Nanoindentation
Based on Oliver Pharr model which assumes that elastic and plastic deformations during loading and only elastic displacements recovered during unloading
Berkovitch tip  β
From P-h curves: max load, max displacement and elastic unloading stiffness
From calibration in FQ (reference material): contact area 
Hardness estimation:
Elastic modulus measurements (derived from eastic contact theory):
Er accounts for elastic displacement in both sample and tip

## Slide 24: qBEI Calibration
When sending a beam of electrons over a sample, electrons interact with atoms, producing various signals (including BE)
BE are electrons from the beam that are reflected back because they are deviated by atom nuclei
Therefore, BE signal is highly sensitive to the local atomic number (Z): the higher the atomic number of the atoms hit by the beam, the higher the BE signal
Bone is a heterogeneous material, composed of varying proportion of:
  Organic matrix: Z ~ 6
  Hydroxylapatite Ca5(PO4)3OH: Z ~ 14.06
The constituent with the highest atomic number dominantly influences the BEs intensity (Ca, Z = 20)

## Slide 25: qBEI Calibration
Adjust machine parameters to get GL of 2 reference materials:
- GL(C) = 25
GL(Al) = 225
Define calibration line with those points
Measure experimentally osteoid GL and fix it as 0 wt% Ca standard
Pure HA is 39.86 wt% Ca, and measure its GL from calibration line (known Zmean = 14.06)
Define standardization line from those points
How can we connect grey level (GL) to local Ca concentration ?
Ca wt% = -4.332 + 0.1733 × GL
Depth resolution : 2 µm

## Slide 26: Distributions (Adults)
LM2
Pl1
LM2
Pl2
LM3
Pl1
LM3
Pl2
LM4
Pl1
LM4
Pl2
LM5
Pl1
LM5
Pl2
LM6
Pl1
LM6
Pl2
LM7
Pl1
LM7
Pl2

## Slide 27: Distributions (Olds)
LM1
Pl1
LM1
Pl2
LM3
Pl1
LM3
Pl2
LM4
Pl1
LM4
Pl2
LM5
Pl1
LM5
Pl2
LM6
Pl1
LM6
Pl2