## Slide 1
H. Souhail1, E. Zamengo2, L. D’Andrea3, S. Blouin2, M.A. Hartmann2, P. Vena3, D. Ruffoni1
University of Liège, Belgium
Ludwig Boltzmann Institute of Osteology, Austria
Politecnico di Milano, Italy
Bone Biomechanics: Microscale
THE MECHANICAL INTERPLAY BETWEEN BONE AND SCAFFOLD MICROSTRUCTURES – A COMPUTATIONAL ANALYSIS

## Slide 2
2
INTRODUCTION METHODS RESULTS CONCLUSIONS
How does the insertion of a bone scaffold impact the mechanical loading on the surrounding bone?
Computational Study
Virtual defect
Virtual implant insertion
Research Question
Toosi et al., 2023, J. Mater. Sci.: Mater. Med.
Rubin et al., 2002, JBMR.
Clinical Context
Servier Medical Art
Bone scaffolds:
Autografts
3D printed
Mechanical interaction in vivo
Servier Medical Art

## Slide 3
3
INTRODUCTION METHODS RESULTS CONCLUSIONS
µ-CT
Images
Radius Model
Voxel size: 24 µm
Defect Model
Computational Cases
Radius
Iliac Crest
INTACT
ILIAC CREST
SCAFFOLD
6mm

## Slide 4
E autograft , E scaffold = 16 GPa
4
INTRODUCTION METHODS RESULTS
Scaphoid
Lunate
Radius
Fz, scaphoid = 60%
Fz, lunate = 40%
U x, y ,z = 0
62 cores on NIC5 SuperComputer ~ 24h
Z
X
Y
ParOSol: Voxel-based parallel micro-FE solver
Simulations
Parameters
1. MICROSTRUCTURE
EFFECT
2. MATERIAL EFFECT
E scaffold = 16 GPa VS 100 GPa
INTRODUCTION METHODS RESULTS CONCLUSIONS
Flaig C. et al., Parallel Comput, 37: 846-854; 2011
Pistoia et al., 2002, J Biomech

## Slide 5
5
INTRODUCTION METHODS RESULTS
Post-Processing
Peri-Implant Bone
Z
X
Y
INTRODUCTION METHODS RESULTS CONCLUSIONS
Mancuso et al., 2020, JBMR
PERI-
SCAFFOLD16
PERI-BONE
PERI-DEFECT
PERI-
AUTOGRAFT
PERI-
SCAFFOLD100

## Slide 6
6
INTRODUCTION METHODS RESULTS CONCLUSIONS

## Slide 7
7
INTRODUCTION METHODS RESULTS CONCLUSIONS
HIGH STRAIN
LOW STRAIN

## Slide 8
8
INTRODUCTION METHODS RESULTS CONCLUSIONS
EFF
HIGH
LOW
PERI-BONE
PERI-DEFECT
PERI-
DEFECT
PERI-
AUTOGRAFT
PERI-
SCAFFOLD
16
PERI-
SCAFFOLD
100
DEFECT
EFFECT
HIGH STRAIN
LOW STRAIN

## Slide 9
9
INTRODUCTION METHODS RESULTS CONCLUSIONS
PERI-AUTOGRAFT
PERI-SCAFFOLD16
SCAFFOLD 16GPa
AUTOGRAFT
EFF
HIGH
LOW
PERI-
DEFECT
PERI-
AUTOGRAFT
PERI-
SCAFFOLD
16
PERI-
SCAFFOLD
100
MICROSTRUCTURE EFFECT
SAME ELASTIC MODULUS!
HIGH STRAIN
LOW STRAIN

## Slide 10
10
INTRODUCTION METHODS RESULTS CONCLUSIONS
EFF
HIGH
LOW
PERI-
DEFECT
PERI-
AUTOGRAFT
PERI-
SCAFFOLD
16
PERI-
SCAFFOLD
100
MATERIAL
EFFECT
PERI-
SCAFFOLD
16
PERI-SCAFFOLD16
SCAFFOLD 16 GPa
PERI- SCAFFOLD100
SCAFFOLD 100 GPa
SAME POROSITY!
HIGH STRAIN
LOW STRAIN

## Slide 11
11
INTRODUCTION METHODS RESULTS CONCLUSIONS
How does the insertion of a bone scaffold impact the mechanical loading on the surrounding bone?
BONE SCAFFOLD
MECHANICAL ENVIRONMENT
STRAIN
SHIELDING
STRAIN
INTENSIFICATION
Microarchitecture
Material
SCAFFOLD DESIGN
In vivo loading

## Slide 12
Hajar Souhail
This work was funded by the European Union’s Horizon Europe (grant agreement no. 101119884).
ACKNOWLEDGMENTS
Prof. P. Vena
L. D’Andrea
PhD
Prof. G. H. van Lenthe
E. Zamengo
PhD Candidate
M.A. Hartmann
Priv. Doz. Dr.
S.Blouin
Senior Researcher
Prof. D. Ruffoni
hsouhail@uliege.be