## Slide 1
v
To explore the impact of different contents of a new type of lipid-polymer (DSPE-PNMVA24) on LNP physicochemical properties (Figure 1) and protein corona formation to then compare it to PEG (DSPE-PEG2000).
Development of safer and efficient LNP formulations for a future antitumoral application.
Degey Manon1, Berger Manon1, Meloni Laura1, Pedergnana Stefano2, Debuigne Antoine2, Jérôme Christine2, Evrard Brigitte1, Maquoi Erik3, Leblond Chain Jeanne4, Piel Géraldine1
1Laboratory of Pharmaceutical Technology and Biopharmacy, University of Liege, CIRM, 15 Avenue Hippocrate, 4000 Liege, Belgium
2Center for Education and Research on Macromolecules CERM, CESAM Research Unit, University of Liege, 13 Allée du Six Août, 4000 Liege, Belgium
3Laboratory of Tumor and Development Biology, GIGA-Cancer, University of Liege, 4000 Liège, Belgium
4CNRS, INSERM, ARNA, University of Bordeaux, UMR 5320, U1212, F-33000 Bordeaux, France
Redesigning lipid nanoparticles for enhanced intravenous delivery for cancer treatment: PNMVA as a promising PEG substitute
[1] L. Schoenmaker et al., ‘mRNA-lipid nanoparticle COVID-19 vaccines: Structure and stability’, Int. J. Pharm., vol. 601, p. 120586, May 2021, doi: 10.1016/j.ijpharm.2021.120586.
[2] M. Berger et al., ‘Poly( N ‐methyl‐ N ‐vinylacetamide): A Strong Alternative to PEG for Lipid‐Based Nanocarriers Delivering siRNA’, Adv. Healthc. Mater., p. 2302712, Nov. 2023, doi: 10.1002/adhm.202302712.
Introduction
Since COVID-19 pandemic, Lipid Nanoparticles (LNPs) encapsulating mRNA have emerged as a new class of therapeutic agent as well as Onpattro®, the first FDA-approved drug based on LNPs and siRNA for a hepatic disease [1]. Indeed, siRNA and mRNA need vectors to reach the target undamaged. This is the reason why LNPs have garnered attention in this context. To target beyond the liver, notably for cancer treatment, LNPs need to be protected from blood biomolecules because of the formation of a protein corona, affecting their efficacy. In this context, polyethylene glycol (PEG) is used to prevent this phenomenon, but its issues initiate the search for alternatives. Recently, alternatives to PEG such as Poly(N-methyl-N-vinylacetamide) (PNMVA) have been studied with LNPs and seem to be promising [2]. However, improvements need to be done to optimize LNP properties and protein corona formation ability.
1.5% 2.5% 3% 4%
DSPE-PNMVA (DP=24)
I. Impact of DSPE-PNMVA24 and DSPE-PEG2000 content on LNP properties
In conclusion, the promising potential of DSPE-PNMVA24 at 4% as an alternative to PEG in LNPs has been confirmed, with findings indicating the need for a higher concentration than previously used.
Figure 2 : Physicochemical properties of different LNP formulations.
II. Impact of DSPE-PNMVA24 and DSPE-PEG2000 content on protein corona formation
Figure 4 : NTA profiles (FBS 33.33%) of different LNP formulations.
Figure 1 : DSPE-PNMVA24 structure.
C18-PEG
C14-PEG
Figure 3 : Illustration of protein corona formation on LNP surface composed of long lipid-PEG (C18) and short lipid-PEG (C14).
Production
The LNPs, produced by rapid-mixing, are composed of CSL3 (switchable lipid), DSPC, cholesterol and different types of C18 lipid-polymers (DSPE-PEG2000 and DSPE-PNMVA24) and DMG-PEG2000 as C14 control at a molar ratio respectively of 50:10:37.5:2.5. The lipid-polymer content was decreased to 1.5% for all the formulations and increased to 3 to 4% by varying the cholesterol content only for DSPE-PEG2000 and DSPE-PNMVA24 formulations.
II. Physicochemical characterization
Key properties such as size, PdI and surface charge were analyzed by DLS and NTA while siRNA encapsulation efficiency was evaluated by Ribogreen® assay. The goal was to meet intravenous administration standards: size < 150 nm, PdI < 0.2 and maximum encapsulation efficiency.
III. Protein corona formation
Protein corona formation was evaluated using NTA method after incubation in 33.33% of FBS at 37°C.
The impact of DSPE-PNMVA24 and DSPE-PEG2000 content (1.5–4%) on LNP physicochemical properties was studied. Increasing the lipid-polymer content reduces Z-average for both LNP types. However, increasing lipid-PEG content increases PdI, while increasing lipid-PNMVA content decreases it. Encapsulation efficiency of siRNA is also changing as increasing lipid-PEG content reduces it, whereas increasing lipid-PNMVA content has no impact. So on, a higher DSPE-PNMVA24 content (4%) is needed to form and stabilize LNPs compared to DSPE-PEG2000. While 1.5% lipid-polymer is used in the COVID-19 vaccines, 4% of DSPE-PNMVA24 ensures LNPs with a size <150 nm, PdI <0.2, and ~80% siRNA encapsulation efficiency (Figure 2).
A previously developed NTA method was used to assess the impact of the nature and lipid-polymer ratio on their ability to protect LNPs from protein corona formation. According to this study, long lipid chains as C18 lipid-PEG protect against protein corona. Indeed, in the presence of 33% of FBS, LNPs covered with 2.5% of this type of lipid-PEG showed no significant variation in size and concentration (Figure 3) at the opposite of LNPs composed of C14 lipid-PEG.
A concentration of 1.5% of DSPE-PEG2000 is sufficient to stabilize LNPs in FBS, maintaining consistent size and concentration over time. In contrast, DSPE-PNMVA24 requires 3–4% to ensure stability, as lower concentrations (<3%) result in irregular size and concentration profiles over time. This indicates that 4% DSPE-PNMVA24 is necessary to enhance shielding capacities (Figure 4).
Results and discussion
Conclusion
Materials and methods
Objectives
III. Preliminary in vitro results : gene knockdownn efficiency (triple negative breast carcinoma MDA-MB-231cells expressing nuclear mEmerald)
The developed formulations were prepared with siGFP a small interfering RNA targeting GFP expression, and incubated with MDA-MB-231 cells expressing mEmerald (mutated form of GFP) for 4 hours in serum-free conditions (100 nM siGFP). Live-cell imaging was performed using the Incucyte Sx5 over 72 hours and showed a decrease of GFP expression with PNMVA formulations inserted at higher contents (Figure 5). Composite images combining phase contrast and green fluorescence are shown. After 72 hours, cells were analyzed by flow cytometry (CytoFLEX) to measure mean fluorescence intensity (MFI) of GFP.
Formulations with 4% DSPE-PNMVA24 allowed the 90% of GFP fluorescence extinction
Figure 5 : Live cell imaging of MDA-MB-231 cells expressing mEmerald after 72 hours of incubation with indicated formulations of LNPs
Untreated cells
CSL3/DSPE-PNMVA24 4% siGFP
References
Notes: Revoir les interprétations des résultats
Revoir les cadres