Supporting Information

Composite polymer electrolytes based on silicon dioxide nanoparticles for lithium metal batteries

Ashish Raj,¥ Bruno Grignard, Ψ, α Maxime Bourguignon, Ψ Christophe Detrembleur, Ψ,ρ and Jean-François Gohy¥ *

¥Institute of Condensed Matter and Nanoscience (IMCN), UCLouvain, Place L. Pasteur 1, 1348 Louvain-la-Neuve, Belgium

ΨCenter for Education and Research on Macromolecules (CERM), CESAM Research Unit, University of Liège, 13 Allée du 6 août, Building B6A, 4000 Liège, Belgium

αFederation of Researcher in Innovation Technologies for CO2 transformation (FRITCO2T research platform), University of Liège, 13 Allée du 6 août, Building B6A, 4000 Liège, Belgium

ρ WEL Research Institute, avenue Pasteur, 6, 1300 Wavre, Belgium

Figure S1: Picture of CSBO-PEO-SiO2 electrolyte membranes with 20 wt% LiTFSI and loaded with different wt% of SiO2 particles.

Figure S2: Picture of PHU-N2N3-SiO2 electrolyte membrane with 20 wt% LiTFSI and 20 wt% of SiO2 particles.

Figure S3: Temperature dependent ionic conductivity for investigated CPEs with VFT Model.

Figure S4: a) Survey spectrum, HR-XPS of b) Oxygen (O1s), and c) Nitrogen (N1s), at the surface lithium anode after cycling with LFP in Li|CSBO-PEO-SiO2 CPE|LFP cell, respectively.

Table S1: Some macroscopic properties of the investigated electrolyte membrane (all loaded with 20 wt% LiTFSI). Adhesion has been qualitatively assessed during peeling off the electrolyte membrane from the mold after drying.

| Sample | CSBO-PEO-10%SiO2 | CSBO-PEO-20%SiO2 | CSBO-PEO-30%SiO2 | PHU-N2N3-20%SiO2 |
| --- | --- | --- | --- | --- |
| Physical nature | Gel-like | Soft solid | Rigid solid | Soft solid |
| Adhesion | Strong | Medium | Weak | Medium |
| Transparency | Transparent | Slightly hazy | Hazy | Transparent |