Supporting Information

In situ generation of highly active sites by chemical vapor deposition of C2H4 over the LaMn0.7Co0.3O3 perovskite for the oxygen reduction reaction

Jhony Xavier Flores-Lasluisa1, Bryan Carré1, Joachim Caucheteux1, Alexandre F. Léonard2, Nathalie Job1

1Department of Chemical Engineering - NCE (Nanomaterials, Catalysis, Electrochemistry), University of Liège, B6a, Allée du six août 11, B-4000 Liège, Belgium

2Department of Chemical Engineering - CARPOR, University of Liège, B6a, Allée du six août 13, B-4000 Liège, Belgium

Figure S.1. XRD patterns of the samples with different CVD times. (a) zoom in the region 25-34º  (b) zoom in the region 38-42º, and (c) zoom in the region 43-47º. (black line ▬) P; (magenta line ▬) CVD_0; (blue line ▬) CVD_10; (olive line ▬) CVD_20; (red line ▬) CVD_30. The asterisk (*) is related to the LaCoO3 structure.

The crystallite sizes were estimated by applying the Scherrer equation [1]:

Dc=kλβcos⁡(θ) 			(Eq. S.1)

where Dc is the crystallite size (nm); k is the constant related to the shape of the grain whose value is 0.89; λ is the wavelength of the radiation source used, which is 0.15406 nm; ꞵ corresponds to the full width at half maximum (FWHM) (radians), and θ is the Bragg angle.

Figure S.2. Raman spectra of the CVD-based composites. (▬) CVD_10; (▬) CVD_20; (▬) CVD_30.

Figure S.3. (a) Thermogravimetric analysis (TGA) curves of the samples and (b) N2 adsorption-desorption isotherms at -196 °C for the samples. (▬) P; (▬) CVD_10; (▬) CVD_20; (▬) CVD_30.

Table S.1. Surface composition of the samples determined by XPS.

| Sample | C | O | La | Mn | Co |
| --- | --- | --- | --- | --- | --- |
|  | wt.% | wt.% | wt.% | wt.% | wt.% |
| P | 17.69 | 21.55 | 50.45 | 7.74 | 2.58 |
| CVD_0 | 17.98 | 25.37 | 50.62 | 4.37 | 1.67 |
| CVD_10 | 58.04 | 17.06 | 22.26 | 2.06 | 0.58 |
| CVD_20 | 74.37 | 8.77 | 14.88 | 1.25 | 0.73 |
| CVD_30 | 70.49 | 11.69 | 15.81 | 1.49 | 0.52 |

Figure S.4. XPS spectra obtained from (a) La 3d; (b) Mn 2p; (c) Co 2p; and (d) O 1s for the pristine perovskite and the composited formed at different times of CVD.

Figure S.5. Cyclic voltammetry experiments performed at different scan rates for the composites in 10 mM K3Fe(CN)6/K4Fe(CN)6 in pH 7.0 PBS solution saturated with N2: (a) CVD_10; (b) CVD_20; (c) CVD_30; and (d) Randles-Sevcik plot obtained from the cyclic voltammetry for samples in the same conditions. (■) CVD_10; (●) CVD_20; (▲) CVD_30.

Figure S.6. (a) Cyclic voltammetry of the pure metal oxides, the composites formed with Vulcan and the CVD_30 sample in 0.1 M KOH under N2 atmosphere and (b) CVs at smaller current density scale to observe only the metal oxides and the composites. Scan rate: 10 mV s-1. (▬) P; (▬) P+Vul; (▬) CVD_0; (▬) CVD_0+Vul; (▬) CVD_30.

Table S.2. Eonset, number of electrons involved in the ORR, limiting current density, and tafel slope obtained from the LSV data of the CVD_30 sample and metal oxides mixed physically with and without Vulcan.

| Sample | Eonseta | E1/2b | ne-c | jlimd | Tafel slopee |
| --- | --- | --- | --- | --- | --- |
|  | V vs. RHE | V vs. RHE | - | mA cm-1 | mV dec-1 |
| P | 0.74 | 0.57 | 3.98 | -2.36 | 150 |
| P+Vul | 0.81 | 0.69 | 3.83 | -4.98 | 74 |
| CVD_0 | 0.65 | 0.56 | 3.20 | -1.00 | 109 |
| CVD_0+Vul | 0.81 | 0.70 | 3.65 | -3.51 | 79 |
| CVD_30 | 0.90 | 0.83 | 3.95 | -3.60 | 54 |

a Eonset: onset potential at -0.1 mA cm2.

b E1/2: half-way potential.

c ne-: the number of electrons at 0.7 V vs. RHE.

d jlim: the current limiting density at 0.4 V vs. RHE.

e Tafel slope.

References

1. 	Waseda Y, Matsubara E, Shinoda K (2011) X-Ray Diffraction Crystallography. Springer Berlin Heidelberg, Berlin, Heidelberg