## Slide 1: Technological characterization of West African iron ores in order to predict their performance in the beneficiation process
Liesbet DUBRON
Eric PIRARD
Arnaud PIRSON

## Slide 2: About Liege
    Liege City
      The cradle of coal mining, steelmaking and zinc metallurgy in Europe...
    Liege University
      A major research partner in Belgium
      4000 researchers; 1800 PhD students
      500+ professors
      Large network of spin off companies ( > 70)
A millenary city

## Slide 3: About Us
  GeMMe
    Minerals Engineering, Materials & Environment
      3 research units; 40+ researchers
        Building materials
        Minerals engineering & recycling
        Georesources & Geo-Imaging
GeMMe operates on the characterization, valorization, transformation, use and recycling of mineral materials at any stage of their life cycle.
A long tradition in Georesources Engineering

## Slide 4: Synopsis
Introduction
Geology of Nimba County
Tokadeh Deposit
  Quantitative Ore Microscopy
Process Mineralogy
  Modal analysis from chemical data
  Inference of optimal beneficiation
Conclusions

## Slide 5: Iron Ore Projects in Liberia and around
After http://www.proactiveinvestors.co.uk (2010)

## Slide 6: Geology of the Nimba Range
  West African Craton

## Slide 7: Geology of the Nimba Range
Nimba Range Geology
  Precambrian basement
    3700 -500 Ma
      Qz-Fsp-Bt gneisses / migmatites
  Supracrustal belts (metamorphic event)
    2750 Ma
      Elongate belts of phyllites, greenstone, schists
  Granitic intrusions (basement + supracrustal)
      Mineralisations  granitic intrusions
  Granite-greenstone association
      Greenstone = metamorphosed/altered mafic volcanic rocks
Berge et al. (1974)

## Slide 8: Geology of the Nimba Range
Nimba Supergroup
  Nimba Itabirite:
    U-shaped series of ridges
      E: Nimba Main Orebody
      S: Bele - Detton - Tokadeh
      NW: Beeton - Gangra - Yuelliton
      N: More Itabirite ranges
  Tokadeh and Yekepa gneisses
    Amphibolite zone in the middle
  Increasing metamorphism from E to W
    E: Upper epidote amphibolite facies
    W: Amphibolite lower-granulite facies
Modified from Berge et al. (1974)

## Slide 9: Tokadeh Deposit
Banded (silicate) iron formation
Upper amphibole to lower granulite metamorphism
Ore Classification

## Slide 10: Quantitative Ore Microscopy
12 classes based on mineralogical phases and textures:
  Monomineralic:
    Pure magnetite (MGT)
    Martite with >50% magnetite (Mar MGT)
    Martite with >50% haematite (Mar HEM)
    Pure haematite (HEM)
    Goethite: varying texture and composition (Goethite)
    Gangue minerals: mainly Qz (Gangue)
  Polymineralic:
    Composite grain MGT/ Gangue
    Composite grain MGT/ Mar- Gangue-Goethite
    Composite grains MGT-HEM
    Composite grains Martite HEM-Gangue
    Composite grain Martite MGT-Gangue
    Composite grain Martite-Goethite

## Slide 11: Quantitative Ore Microscopy
53% Fe
45% Fe
36% Fe
Chart: 
| MGT | Martite MGT | Martite HEM | Composite grain MGT- Gangue | Composite grain MGT/Mar-Gangue-Goethite | Composite grain Martite HEM-Gangue | Composite grain Martite MGT-Gangue | Composite grain Martite-Goethite | Goethite | Gangue
 | 0.12752 | 0.32993 | 0.27072 | 0.0079352 | 0.067691 | 0.037922 | 0.042411 | 0.07324 | 0.018673 | 0.021768
Chart: 
| MGT | Martite MGT | Martite HEM | HEM mono/polycrystalline | Composite grain MGT/Mar-Gangue-Goethite | Composite grain MGT-HEM monocrystalline | Composite grain Martite HEM-Gangue | Composite grain Martite-Goethite | Goethite | Gangue
 | 0.050001 | 0.23034 | 0.41011 | 0.021533 | 0.039861 | 0.011362 | 0.0098859 | 0.11563 | 0.045733 | 0.061014
Chart: 
| MGT | Martite MGT | Martite HEM | Composite grain MGT- Gangue | Composite grain MGT/Mar-Gangue-Goethite | Composite grain Martite HEM-Gangue | Composite grain Martite MGT-Gangue | Composite grain Martite-Goethite | Goethite | Gangue
 | 0.28677 | 0.30568 | 0.22908 | 0.028127 | 0.012342 | 0.013711 | 0.032067 | 0.045826 | 0.011776 | 0.030681
OX
UT
LT

## Slide 12: Quantitative Ore Microscopy
Tokadeh iron ore profile:
  Downward increase of magnetite
  Upward increase of martite, hematite and goethite
Chart: 
| Soft Oxide | Upper Transition | Lower Transition
Magnetite | 0.050001 | 0.12951 | 0.28677
Hematite | 0.021533 | 6.7716e-05 | 0.0023911
Martite (HEM) | 0.41011 | 0.27072 | 0.22908
Goethite total | 0.16136 | 0.091913 | 0.057601

## Slide 13: Quantitative Ore Microscopy
Tokadeh iron ore profile:
  Upper transition zone:
    High level of composite grains
    Low degree of liberation Fe-phase and gangue
Chart: 
| Soft Oxide | Upper Transition | Lower Transition
Gangue | 0.061014 | 0.021768 | 0.030681
All Composite grains (Fe-phase + gangue) | 0.052762 | 0.15596 | 0.086247

## Slide 14: Process Mineralogy
Tokadeh samples from all 3 zones (OX UT, LT)
Spiral concentrates
  Chemical analysis
  Optical microscopy
  XRD
Simulation behaviour during mineral processing
  Expected Optimal Beneficiation

## Slide 15: Process Mineralogy
 | Total (/100%)
Magnetite | 29,7 %
Haematite | 50,0 %
Goethite | 15,8 %
Gangue | 4,5 %
Mineral species confirmed by XRD
Quantitative Mineralogy from Chemical Data:

## Slide 16: Process Mineralogy
Quantitative Mineralogical Analysis
  Constrained by microscopy / XRD
Limits:
Kenomagnetite has not been considered.
Potential contaminations of goethite by silica, alumina and manganese have not been considered.
Mineralogical Analysis of Spiral Concentrates obtained for the 3 different ores

## Slide 17: Process Mineralogy
Inference of magnetic separation concentrates from modal analysis:

## Slide 18: Process Mineralogy
Theoretical upgrading potential
Estimated modal analysis of concentrates after an additional magnetic separation
Potential upgrading of spiral concentrates by magnetic separation.

## Slide 19: Conclusions
Liberia hosts several world class deposits
Importance of mineralogical data at exploration stage
Simple estimates of quantitative mineralogy can (often) be obtained by combining microscopy, chemistry & XRD
Understanding of mineral beneficiation
Inference of optimal beneficiation

## Slide 20: Thank You