Supplementary data

Optimisation of dynamic headspace sampling conditions for the identification of Palaeolithic adhesives

Anika Lokker1, Pierre-Hugues Stefanuto1, Dries Cnuts2, Veerle Rots2,3*, Jean-Francois Focant1*

1 –  University of Liège, Organic and Biological Analytical Chemistry Group, Allée du 6 Août 11, Quartier Agora, Sart-Tilman, Liège 4000, Belgium

2 – University of Liège, TraceoLab/Prehistory, Quai Roosevelt 1B, Liège 4000, Belgium

3 – F.R.S-FNRS, Brussels, Belgium

Corresponding author: alokker@uliege.be (A. Lokker)

*co-last

S2.1 The preparation of hide glue

Hide glue was made from a fresh deer hide. The first step was removing of the blood, meat and fat from the hide by scraping. Then, the hair was removed by immersion of the hide in water with (wood) ash for 2 to 3 days, when the hair has come loose it was easily removed by scraping. The cleaned hide was cut into small pieces and immersed under water again. The hydrolysis of the hide took place at a temperature between 70-75°C for 10 hours. After this time, the hide was transformed to a sticky substance. The glue was spread out in a thin layer and left to cool. The dried glue was cut into pieces and stored for later use.

For the headspace measurement, 10 mg of dried flakes was weighted and dissolved in a few droplets of MilliQ water at room temperature. The mixture was left to stand overnight and the next day a gluey substance was obtained. On this substance the HS-SPME and DHS measurements were performed.

| Experiment | Tinc | Timeinc | Vpurge | Fpurge | Response value (total area) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | HCMT | OXMT | HCST | OXST |
| 1 | 30 | 10 | 300 | 15 | 7.63E+08 | 5.03E+07 | 1.05E+07 | 0.00E+00 |
| 2 | 50 | 10 | 300 | 15 | 4.04E+08 | 1.72E+08 | 3.19E+07 | 2.94E+06 |
| 3 | 30 | 30 | 300 | 15 | 3.08E+08 | 2.80E+07 | 8.11E+06 | 1.67E+05 |
| 4 | 50 | 30 | 300 | 15 | 4.80E+08 | 2.47E+08 | 3.91E+07 | 3.07E+06 |
| 5 | 30 | 10 | 600 | 15 | 5.51E+08 | 9.03E+07 | 2.20E+07 | 1.12E+06 |
| 6 | 50 | 10 | 600 | 15 | 6.88E+08 | 3.36E+08 | 8.53E+07 | 8.79E+06 |
| 7 | 30 | 30 | 600 | 15 | 4.61E+08 | 4.70E+07 | 7.63E+06 | 3.90E+05 |
| 8 | 50 | 30 | 600 | 15 | 4.25E+08 | 4.19E+08 | 5.59E+07 | 6.40E+06 |
| 9 | 30 | 10 | 300 | 30 | 4.19E+08 | 2.78E+07 | 6.09E+06 | 1.14E+06 |
| 10 | 50 | 10 | 300 | 30 | 5.59E+08 | 2.02E+08 | 3.56E+07 | 3.96E+06 |
| 11 | 30 | 30 | 300 | 30 | 6.52E+08 | 6.01E+07 | 1.89E+07 | 2.08E+05 |
| 12 | 50 | 30 | 300 | 30 | 5.96E+08 | 2.20E+08 | 3.16E+07 | 9.53E+05 |
| 13 | 30 | 10 | 600 | 30 | 2.77E+08 | 1.34E+07 | 5.19E+06 | 1.02E+05 |
| 14 | 50 | 10 | 600 | 30 | 4.47E+08 | 2.89E+08 | 3.78E+07 | 4.97E+06 |
| 15 | 30 | 30 | 600 | 30 | 5.85E+08 | 1.20E+08 | 2.86E+07 | 7.97E+05 |
| 16 | 50 | 30 | 600 | 30 | 4.08E+08 | 1.47E+08 | 4.13E+07 | 3.01E+06 |
| 17 | 40 | 20 | 450 | 22.5 | 7.53E+08 | 1.68E+08 | 5.73E+07 | 1.96E+06 |
| 18 | 40 | 20 | 450 | 22.5 | 6.80E+08 | 2.35E+08 | 4.83E+07 | 1.30E+06 |
| 19 | 40 | 20 | 450 | 22.5 | 5.30E+08 | 1.24E+08 | 2.55E+07 | 1.94E+06 |

Table S1. Experimental values and response values of the FFD runs.